## PDF Card. PDF Number; 00-021-1272; Status; Primary; Quality Mark; Star. Pressure/Temperature; Ambient. Chemical Formula; Ti O2. Structural Formula. Empirical Formula; O2 Ti. Weight %; O40.06 Ti59.94. Atomic %; O66.67 Ti33.33. Compound Name; Titanium Oxide. ANX. Mineral Name; Anatase, syn. Also Called. Experimental; Rad; ; Filter; d-Spacing; Cutoff; Intensity; I/Ic. 3.3. Camera Diameter. Physical; SYS; Space Group; Aspect; Cell Wave Vector 1; Cell Wave Vector 2. Tetragonal; I41/amd (141). Subsystems; ID; W Matrix.. Author's Cell; a; b; c; ; ; . 3.7852; 9.5139. Volume; Z; Molecular Volume/Formula Unit Volume. 136.31; 4.00; 34.08. Author's Cell Axial Ratio; c/a; a/b; c/b. 2.513. Density; Dcalc; Dmeas; Dstruc. 3.893. SS/FOM; Temperature; Melting Point; R-factor; Error. F(30) = 74.5(0.0115, 35); 298.000. Crystal; Space Group; Molecular Weight. I41/amd (141); 79.90. Crystal Data; a; b; c; ; ; . 3.785; 3.785; 9.514; 90.00; 90.00; 90.00. Volume; Z. 136.31; 4.00. Crystal Data Axial Ratio; c/a; a/b; c/b. 2.514; 1.000; 2.514. Reduced Cell; a; b; c; ; ; . 3.785; 3.785; 5.458; 110.29; 110.29; 90.00. Volume. 68.16. Optical; ; n; ; Sign; 2V. Structure; Atomic parameters are cross-referenced from PDF entry 04-007-0701. ADP Type; U. Origin; O1. Crystal (Symmetry Allowed); Centrosymmetric. SG Symmetry Operators; Seq; Operator. 1; x,y,z. 2; -x+1/2,-y+1/2,z+1/2. 3; x+1/2,y,-z+3/4. 4; -x,-y+1/2,-z+1/4. 5; -x,y,z. 6; x+1/2,-y+1/2,z+1/2. 7; -x+1/2,y,-z+3/4. 8; x,-y+1/2,-z+1/4. 9; y+1/2,x+1/2,-z+1/2. 10; -y,-x,-z. 11; y,x+1/2,z+1/4. 12; -y+1/2,-x,z+3/4. 13; -y+1/2,x+1/2,-z+1/2. 14; y,-x,-z. 15; -y,x+1/2,z+1/4. 16; y+1/2,-x,z+3/4.. SG Symmetry Operators (Modulated Structure); Seq; Operator.. Atomic Coordinates; Atom; Num; Wyckoff; Symmetry; x; y; z; SOF; Uiso; AET. Ti; 1; 4a; -4m2; 0.0; 0.0; 0.0; 1.0; 0.0058; 6-a. O; 2; 8e; 2mm.; 0.0; 0.0; 0.20806; 1.0; 0.0072; 3#b.. Atomic Coordinates (Modulated); Atom; Num; x; y; z; SOF; Uiso; Subsys.. Anisotropic Displacement Parameters; Atom; Num; Uani11; Uani22; Uani33; Uani12; Uani13; Uani23. Ti; 1; 0.0052; 0.0052; 0.007; 0.0; 0.0; 0.0. O; 2; 0.0117; 0.0027; 0.0072; 0.0; 0.0; 0.0.. Anisotropic Displacement Parameters (Modulated); Atom; Num; Uani11; Uani22; Uani33; Uani12; Uani13; Uani23.. Modulated. Positional Displacement Parameters; Atom Site; Axis; WV ID; Cos; Sin.. Atomic Displacement Parameters; Atom Site; WV ID; Cos; Sin; Tensor El... Occupation Modulation; Atom Site; WV ID; Cos; Sin.. Occupational - Crenel; Atom Site; C; W.. Displacement - SawTooth; Atom Site; C; W; AX; AY; AZ.. Miscellaneous; CAS Number. Pearson; tI12.00. Pearson w/o H. Subfile Indicator; Mineral Related (Mineral , Synthetic), Common Phase, Forensic, Metals & Alloys, Pigment/Dye, Educational Pattern, Inorganic, NBS Pattern, Pharmaceutical (Excipient), Primary Pattern. Prototype Structure; Ti O2. Prototype Structure (Alpha Sort). LPF Prototype Structure; Ti O2,tI12,141. LPF Prototype Structure (Alpha Sort). Mineral Classification. Zeolite Classification. Entry Date. Last Modification Date; 01/11/2013. Former PDF #. Cross-Reference PDF #'s; 00-001-0562 (Deleted), 01-071-1166 (Alternate), ✓ 04-001-7641 (Alternate), ✓ 04-002-2678 (Alternate), ✓ 04-002-2750 (Alternate), ✓ 04-002-2751 (Alternate), ✓ 04-002-8296 (Alternate), ✓ 04-006-1918 (Alternate), ✓ 04-006-9240 (Alternate), ✓ 04-007-0701 (Alternate). References; Type; DOI; Reference. Primary Reference; Natl. Bur. Stand. (U. S. ) Monogr. 25 7, 82 (1969).. Crystal Structure; Crystal Structure Source: LPF... Comments; Database Comments; Additional Patterns: See PDF 01-071-1166. Validated by calculated pattern. Color: Colorless. General Comments: Pattern reviewed by Holzer, J., McCarthy, G., North Dakota State Univ, Fargo, North Dakota, USA, ICDD Grant-in-Aid (1990). Agrees well with experimental and calculated patterns. Polymorphism/Phase Transition: Anatase and another polymorph, brookite (orthorhombic), are converted to rutile (tetragonal) by heating above 700 C. Sample Source or Locality: Sample obtained from National Lead Co., South Amboy, New Jersey, USA. Temperature of Data Collection: Pattern taken at 298 K. Unit Cell Data Source: Powder Diffraction.. User Comments. Shared Comments. ## d-Spacings.  =1.54056. ## 00-021-1272 (Fixed Slit Intensity) 2; d(Å); Intensity; h; k; l; m; n; o; *. 25.2806; 3.520000; 100; 1; 0; 1. 36.9459; 2.431000; 10; 1; 0; 3. 37.8002; 2.378000; 20; 0; 0; 4. 38.5750; 2.332000; 10; 1; 1; 2. 48.0487; 1.892000; 35; 2; 0; 0. 53.8897; 1.699900; 20; 1; 0; 5. 55.0602; 1.666500; 20; 2; 1; 1. 62.1190; 1.493000; 4; 2; 1; 3. 62.6884; 1.480800; 14; 2; 0; 4. 68.7601; 1.364100; 6; 1; 1; 6. 70.3087; 1.337800; 6; 2; 2; 0. 74.0289; 1.279500; <2; 1; 0; 7. 75.0294; 1.264900; 10; 2; 1; 5. 76.0173; 1.250900; 4; 3; 0; 1. 80.7249; 1.189400; <2; 0; 0; 8. 82.1361; 1.172500; 2; 3; 0; 3. 82.6594; 1.166400; 6; 2; 2; 4. 83.1465; 1.160800; 4; 3; 1; 2. 93.2174; 1.060000; 2; 2; 1; 7. 94.1783; 1.051700; 4; 3; 0; 5. 95.1394; 1.043600; 4; 3; 2; 1. 98.3152; 1.018200; 2; 1; 0; 9. 99.8007; 1.007000; 2; 2; 0; 8. 101.2175; 0.996700; 2; 3; 2; 3. 107.4437; 0.955500; 4; 3; 1; 6. 108.9585; 0.946400; 4; 4; 0; 0. 112.8361; 0.924600; <2; 3; 0; 7. 113.8569; 0.919200; 2; 3; 2; 5. 114.9041; 0.913800; 2; 4; 1; 1. 118.4341; 0.896600; 4; 2; 1; 9. 120.0989; 0.889000; 2; 2; 2; 8. 121.7200; 0.881900; <2; 4; 1; 3. 122.3307; 0.879300; 2; 4; 0; 4. 131.0290; 0.846400; 2; 4; 2; 0. 135.9910; 0.830800; <2; 3; 2; 7. 137.3839; 0.826800; 4; 4; 1; 5. 143.8785; 0.810200; 2; 3; 0; 9. 150.0282; 0.797400; 4; 4; 2; 4. 152.6219; 0.792800; 2; 0; 0; 12. © 2013 International Centre for Diffraction Data. All Rights Reserved