IXS at Extreme Pressure and Temperature of the APS

2018 COMPRES Annual Report, November 2017 – October 2018

Prepared by:  Wenli Bi (COMPRES researcher)

Ercan Alp (ANL) and Jay Bass (UIUC) (PI)

Jiyong Zhao, Michael Hu, Ahmet Alatas, Thomas Toellner, Ayman Said (ANL-

APS staff)

Overview

The inelastic x-ray scattering (IXS) at extreme temperature (between 4 and 3500 K) and high pressures is a unique capability provided to COMPRES Users through General User Proposals as well as a COMPRES Partner User Program at the APS 3-ID and 30-ID beamlines.

The capability involves access to two types of instruments: i) nuclear resonant scattering at 3-ID-B, 3-ID-D, and 30-ID-B, and ii) HERIX-3 and HERIX-30, the High Energy Resolution Inelastic X-Ray Spectrometers at 3-ID-C and 30-ID-C, respectively.

These special capabilities involve

- A micro-focused beam with 10 microns in beam size at 3-ID-B, 17 microns in beam size at 3-ID-C, and about 30 microns at 30-ID-B and 30-ID-C.

- 1 meV or better resolution monochromators for 57Fe, 119Sn, 151Eu, 161Dy, 83Kr Mössbauer isotopes, and cryogenically cooled high-resolution monochromators at 21.65 keV for the HERIX-3 and 23.71 keV for the HERIX-30 spectrometers.

- On-line Ruby systems at 3-ID-B and 30-ID-C for in-situ pressure measurement and offline Raman system at Sector 3 laboratory area.

- DACs of various design for synchrotron Mössbauer experiments, and screw- and membrane-type panoramic DAC’s for nuclear resonant inelastic x-ray scattering experiments with compatible gas loading gearboxes for gas loading at GSECARS.

- Cryogenically cooled cryostat and superconducting magnet (7T) suitable for cooling samples under pressure for magnetism studies.

- Combined inelastic spectrometer/x-ray diffraction capabilities for single-crystal structure and orientation determination inside the DAC at HERIX-3 and HERIX-30 spectrometers.

- Combined nuclear resonant inelastic spectrometer with Mössbauer spectroscopy and x-ray diffraction capabilities for atomic and electronic structure determination, and equation-of-state measurements at 3-ID-B.

- High-temperature double-sided fiber IR- laser heating capability to reach above 3500 K, and internal resistive heating capability to reach 1000 K. Includes spectroradiometric temperature measurements determined from CCD and FasTeR system at 3-ID-B.

In addition to these synchrotron-based capabilities, we offer an offline conventional Mössbauer spectroscopy (CMS) laboratory with two Mössbauer drives as an additional resource, which is being used with steadily increasing frequency by COMPRES researchers. With the availability of point-sources, Mössbauer data can be taken from samples at high pressure inside a DAC or recovered/synthesized samples after/from high-pressure experiments.

Scientific Highlights

- Strongly anisotropic magnesiowüstites in Earth’s lower mantle

The juxtaposition of a liquid iron‐dominant alloy against a mixture of silicate and oxide minerals at Earth's core‐mantle boundary is associated with a wide range of complex seismological features. One category of observed structures is ultralow‐velocity zones, which are thought to correspond to either aggregates of partially molten material or solid, iron‐enriched assemblages. Phonon dispersion relations of magnesiowüstite containing 76 mol % FeO, a candidate ultralow‐velocity zone phase, were measured under high pressure at Sector 30 using the high-energy resolution inelastic x-ray scattering (HERIX). These measurements show that magnesiowüstite becomes strongly elastically anisotropic with increasing pressure, potentially contributing to a significant proportion of seismic anisotropy detected near the base of the mantle (Finkelstein et al., J. Geophys. Res., 123, 4740-4750, 2018).

- Experimental constrains on the sound velocities of cementite Fe3C to core pressures

﻿Sound velocities of cementite Fe3C have been measured up to 1.5 Mbar and at 300 K in a diamond anvil cell using the nuclear resonant inelastic X-ray scattering (NRIXS) technique. From the partial phonon density of states (pDOS) and equation of state (EOS) of Fe3C, we derived its elastic parameters including shear modulus, compressional (VP) and shear-wave (VS) velocities to core pressures. A pressure-induced spin-pairing transition in the powdered Fe3C sample was found to occur gradually between 10 and 50 GPa by the X-ray Emission Spectroscopy (XES) measurements. Following the completion of the spin- pairing transition, the VP and VS of low-spin Fe3C increased with pressure at a markedly lower rate than its high-spin counterpart. Our results suggest that the incorporation of carbon in solid iron to form iron carbide phases, Fe3C and Fe7C3, could effectively lower the VS but respectively raise the Poisson’s ratio by 0.05 and 0.07 to approach the seismically observed values for the Earth’s inner core. The comparison with the preliminary reference Earth model (PREM) implies that an inner core composition containing iron and its carbon-rich alloys can satisfactorily explain the observed seismic properties of the inner core (Chen et al., Earth Planet. Sci. Lett. 494, 164-171, 2018).

- Valence and spin states of bridgmanite in Earth’s lower mantle

﻿Heterogeneity in Earth’s mantle is a record of chemical and dynamic processes over Earth’s history. The geophysical signatures of heterogeneity can only be interpreted with quantitative constraints on effects of major elements such as iron on physical properties including density, compressibility, and electrical conductivity. However, deconvolution of the effects of multiple valence and spin states of iron in bridgmanite (Bdg), the most abundant mineral in the lower mantle, has been challenging. Combining synchrotron Mössbauer spectroscopy, x-ray emission spectroscopy, x-ray diffraction, and electrical resistivity experiments on a ferric-iron-only (Mg0.46Fe3+0.53)(Si0.49Fe3+0.51)O3 Bdg, it is shown that Fe3+ in the octahedral site undergoes a spin transition between 43 and 53 GPa at 300 K. The resolved effects of the spin transition on density, bulk sound velocity, and electrical conductivity are smaller than previous estimations, consistent with the smooth depth profiles from geophysical observations. For likely mantle compositions, the valence state of iron has minor effects on density and sound velocities relative to major cation composition (Liu et al., Nat. Commun. 9, 1284, 2018).

- ﻿High-pressure geophysical properties of fcc phase FeHx

Within the known iron hydride phase diagram, the face‐centered cubic (fcc) structure is considered the most stable structure at high temperatures, rendering it more important for extrapolation to core P-T conditions than the bcc and hcp structures. Face centered cubic (fcc) FeHX was synthesized at pressures of 18–68 GPa and temperatures exceeding 1,500 K. Thermally quenched samples were evaluated using NRIXS and synchrotron X-ray diffraction to determine sample composition and sound velocities to 82 GPa. To aid in the interpretation of nonideal (x ≠ 1) stoichiometries, two equations of state for fcc FeHX were developed, combining an empirical equation of state for iron with two distinct synthetic compression curves for interstitial hydrogen. Matching the density deficit of the Earth’s core using these equations of state requires 0.8–1.1 wt % hydrogen at the core-mantle boundary and 0.2–0.3 wt % hydrogen at the interface of the inner and outer cores. Furthermore, a comparison of Preliminary Reference Earth Model (PREM) to a Birch’s law extrapolation of our experimental results suggests that an iron alloy containing ~0.8–1.3 wt% hydrogen could reproduce both the density and compressional velocity (VP) of the Earth’s outer core (Thompson et al., Geochemistry, Geophys. Geosystems. 19, 305-314, 2018).

Beamline Personnel

The 3-ID beamline is owned and operated by the X-ray Science Division of the Advanced Photon Source (APS), Argonne National Laboratory. There are 5 full-time staff scientists paid by the APS, and a Senior Spectroscopist researcher (Wenli Bi), jointly funded by COMPRES (60%) and the APS (40%). In addition, the beamline has full access to APS’s technical and engineering support system. The group is part of the Inelastic X-Ray and Nuclear Resonant Scattering (IXN) group, led by Dr. Thomas Gog, who reports to Dr. Jonathan Lang, the Director of XSD at the APS.

Beamline Operations

Experiments are performed at the 3-ID and 30-ID beamlines based on general user proposals (GUP’s). The oversubscription rate at 3-ID is about 2.  During the period of this report, there were 52 and 11 GUP requests from Earth Science and high-pressure research groups for 3-ID and 30-ID, respectively. Of these GUP requests 32 (62 % of the total requests) and 8 (73 %) were granted beam time at Sectors 3-ID and 30-ID, respectively. These percentages are well above the average acceptance rate, which is below 40%. The relatively high success rates for COMPRES proposals are due to the excellent quality of research that these techniques attract from the COMPRES community as well as the close collaboration between the beamline staff and COMPRES user groups to develop effective proposals that are highly competitive for beam time. During the last year, 21 geosciences and high pressure user groups have been allocated beam time. About 18 graduate students and 14 postdocs participated experiments at 3-ID and 30-ID.

The offline Mössbauer lab provides mail-in service for COMRPES users for beamline related experiments as well as individual sample characterization. It has been in high demand. During the last year over 30 samples from 13 COMPRES groups have been measured.

The offline Raman system has been used routinely by users from Sector 3 and other beamlines, after the relocation from Sector 13 to Sector 3 in June 2016. During the last year, the Raman system has been used by 15 groups for pressure measurements by either ruby fluorescence or diamond Raman edge methods, as well as characterizing samples by Raman spectroscopy.

During the last three years the share of NRS beamtime at 3-ID has gone up from 60 to 80% with the application of the hybrid filling mode at APS. Furthermore, 10% additional beam time is now allocated for 119Sn experiments at Sector 30, which reduces the burden on Sector 3 and allows more time for COMPRES users. Additionally, due to relocation of the MERIX instruments previously at Sector 30 to Sector 27 the total time for IXS measurements between sector 3 and 30 has gone up from 70% to 90%.

Performance Metrics

In the period of this report 20 groups from geosciences/COMPRES community were allocated beam time at 3-ID and 30-ID. The average time allocated for COMPRES users is ~50% of the total available beam time. Detailed information of the allocation is listed in the Appendix.

Beamline Community Activities

- Organized the NRS Workshop 2018: Nuclear Resonant Inelastic X-ray Scattering and Data Analysis, Nov. 2-4, 2018 at the Advanced Photon Source, Argonne National Laboratory. The workshop was jointly funded by COMPRES and APS. The two-and-half days workshop was again a great success with 27 participants actively engaged in the lecture and hands-on training sessions with PHOENIX.

- Active participation in the COMPRES annual meeting with oral presentations and posters.

- Organized the NRS 2017 workshop: CONUSS and Synchrotron Mössbauer data analysis, Nov. 16-19, 2017, APS, ANL.

- Year-round training of users for beamline experiment operation and data analysis.

- Offered mail-in service to COMPRES users at the Mössbauer lab.

- Beamline staff is heavily involved in beam time proposal writing, experiment planning, diamond anvil cell preparation, sample loading, beamline experimental setup, data collection, data analysis and interpretation, and manuscript writing in collaboration with users.

Beamline Development

- Acquired and commissioned an in-vacuum horizontal bending mirror at 3ID-D for 10 micron focusing size (APS funds). This is a critical development for high pressure experiments at 3ID-D, especially to utilize the anticipated fast shutter system at 3ID.

- Designed and procured components for an online Raman system to allow online pressure measurements from diamond Raman edge and in-situ Raman measurements from sample in diamond anvil cell.

- Renewed the CCD cameras for the temperature readout system of the online laser heating system (with APS fund).

- Purchased two One-20 DACs with wide opening angle (120 degrees) to allow access of the high angle reflection in HERIX experiments (with APS funds).

- Acquired two more symmetric DACs for synchrotron Mössbauer, HERIX and x-ray diffraction experiments (with APS funds).

- High pressure RIXS experiment is routinely carried out at Sector 27, a potential capability that can be explored by the COMPRES community to investigate electronic structure under pressure.

Planned Activities

Sector 3 and Sector 30 have a steady flow of users from the COMPRES community, notably including beamtime requests from new users. The main activity of this project will continue to be service to COMPRES users by the Senior Spectroscopist, Dr. Wenli Bi. Wenli helps users write GUP proposals for beamtime, prepare experiments, help and instruction on sample and diamond cell preparation, collects NRS data, performs conventional Mossbauer experiments and data analysis for mail-in and drop-off users. Dr. Bi is involved with a great deal of one-on-one training of students and other users in all aspects of experiments at the beamlines, even including basic training on use of diamond cells. In addition, the following activities are planned for the next year of the APS and COMPRES funding, including education and outreach as the last two items:

- We are building an online Raman system for in-situ pressure measurements for experiments above 30 GPa and for taking Raman spectra simultaneously on samples. We have acquired all the major components (laser, CCD, spectrometer, grating, etc.). The new online Raman system is expected to be completed and installed early next year.

The total cost of the complete system is approximately $75 K. COMPRES contributed $56,375 for the detector and spectrometer and APS contributed ~$19,000 for components including laser, optics and motors.

- Workshop on Nuclear Resonant Scattering and Data Analysis, November, 2019.

- NRS pre-meeting workshop at COMRPES annual meeting, August, 2019

Budget Request for June 2019 – May 2020

| Expense | COMPRES request | ANL contribution |
| --- | --- | --- |
| Salary, Dr. Wenli Bi | 52,057 | 34,705 |
| Fringe Benefits (41.98%) | 21,853 | 14,569 |
| Domestic Travel | 6,150 |  |
| Materials & Supplies | 1,558 |  |
| Conference Registration Fees | 900 |  |
| Indirect Costs (26%) | 21,455 | 12,811 |
| Total | $103,973 | $62,085 |

Budget Justification

Salary is requested (60%=7.2 months) for the Research Spectroscopist, Dr. Wenli Bi, who is devoted 100% to the project and resides full time at the APS, Argonne National Laboratory (Argonne).

Fringe Benefits for the academic salary of Dr. Wenli Bi is at the negotiated rate of 41.98%.

Domestic Travel:  We request funds for Wenli Bi to attend one domestic scientific conference (e.g., the American Geophysical Union (AGU) annual meeting) and the COMPRES annual meeting. Estimates are based on historical data for 6 days and 5 nights lodging, per diem, airfare, and local transport for a conference, and 4 days and 3 nights for the COMPRES Annual Meeting.

Jay Bass as PI will travel to the APS to collaborate and facilitate the research. We budget for 3 trips covering vehicle mileage and lodging. Funds are requested for Bass to attend the COMPRES annual meeting (transportation, lodging).

Materials & Supplies:  Dr. Wenli Bi is encouraged as a COMPRES research scientist to pursue experiments for her career development, and is expected to do experiments leading to the development of new techniques for high pressure at her beamline. Accordingly, requested funding includes materials and supplies for experiments by synchrotron and off-line Mossbauer users and the Research Spectroscopist. Such supplies include but are not limited to reagents, rhenium and other metal foils for gaskets, diamond anvil seats, 57Fe metal (to make samples for Mossbauer experiments), and custom sample holders.

User Satisfaction

Please find the attached file titled “End_of_experiment_questionnaire_3ID_2018”. Please note that not all the users filled out the end of experiment form.

Appendices

- List of publications

- Solomatova N.V., Alieva A., Finkselstein G.J., Sturhahn W., Baker M.B., Beavers C.M., Zhao J., Toellner T.S., and Jackson J.M., High-pressure single-crystal X-ray diffraction and synchrotron Mössbauer study of monoclinic ferrosilite, Comptes Rendus Geoscience, (in press) 2018.

- Finkelstein G.J., Jackson J.M., Said A., Alatas A., and Leu B.M., Sturhahn W., and Toellner T.S., Strongly anisotropic magnesiowüstite in Earth's lower mantle, J. Geophys. Res., 123, 4740-4750, 2018.

- Prissel K.B., Krawczynski J.M., Nie N.X., Dauphas N., Couvy H., Hu M.Y., Alp E.E., Roskosz M., Experimentally determined effects of olivine crystallization and melt titanium content on iron isotope fractionation in planetary basalts, Geochim. Cosmochim. Acta 238, 580, 2018.

- Chen B., Lai X., Li J., Liu, J., Zhao J., Bi W., Alp E. E., Hu M. Y. & Xiao Y., Experimental constraints on the sound velocities of cementite Fe3C to core pressures, Earth Planet. Sci. Lett. 494, 164-171, 2018.

- Klein R. A., Walsh J. P. S., Clarke S. M., Guo Y., Bi W., Fabbris G., Meng Y., Haskel D., Alp E. E., Duyne R. P. Van, Jacobsen S. D. & Freeman D. E., Impact of pressure on magnetic order in jarosite, J. Am. Chem. Soc. 140, 12001, 2018.

- Materne P., Bi W., Alp E.E., Zhao J., Hu M. Y., Jesche A., Geibel C., Kappenberger R., Aswartham S., Wurmehl S., Büchner B., Zhang D., Goltz T., Spehling J. & Klauss H. Phys. Rev. B. 98, 14517, 2018.

- Thompson E.C., Davis A. H., Bi W., Zhao J., Alp E. E., Zhang D., Greenberg E., Prakapenka V. B. & Campbell A. J., High-pressure geophysical properties of fcc phase FeHx,  Geochemistry, Geophys. Geosystems. 19, 305-314, 2018.

- Fei Y., Iqbal M., Kong S. D., Xue Z., McFadden C. P., Guillet J. L., Doerrer L. H., Alp E. E., Bi W., Lu Y., Dandamudi C. B., Ranganath P. J., Javier K. J., Ahmadian M., Ellison C. J. & Johnston K. P., Aqueous Superparamagnetic magnetite dispersions with ultrahigh initial magnetic susceptibilities, Langmuir. 34, 622–629, 2018.

- Liu J., Dorfman S. M., Zhu F., Li J., Wang Y., Zhang D., Xiao Y., Bi W. & Alp, E. E., Valence and spin states of iron are invisible in Earth’s lower mantle, Nat. Commun. 9,1284, 2018.

- Y. Hong, Lin J-F., Hu M.Y., Roskosz M., Bi W., Zhao J., Alp E.E., Liu J., Liu J., Wentzowitch R.M., Okuchi T., Dauphas N., Iron isotopic fractionation in mineral phases from earth’s lower mantle: did terrestrial magma ocean crystallization fractionate iron isotopes? Earth Planet. Sci. Lett. (in press) 2018.

- Materne P., Bi W., Alp E.E., Zhao J., Hu M. Y., Jesche A., Geibel C., Kappenberger R., Aswartham S., Wurmehl S., Büchner B., Zhang D., Goltz T., Spehling J. & Klauss H., Bandwidth controlled insulator-metal transition in BaFe2S3: a Mössbauer study under pressure, Phys., Rev. B (under review) 2018.

- Materne P., Bi W., Zhao J., Hu M.Y., Alp E. E., Kappenberger R., Aswartham S., Wurmehl S., Büchner B., Microscopic phase diagram of LaFeAsO single crystals under pressure, Phys. Rev. B (accepted) 2018.

- Zhao J. Y., Bi W., Sinogeikin S., Hu M.Y., Alp E. E., Lin J. F., Jin C. Q., A compact membrane-driven diamond anvil cell and cryostat system for nuclear resonant scattering at high pressure and low temperature, Rev. Sci. Instrum. 88, 125109, 2017.

- Dauphas N., Hu M.Y., Baker E.M., Hu J., Tissot F.L.H., Alp E.E., Roskosz M., Zhao J., Bi W., Liu J., Lin J-F., Nie N.X., Heard A., SciPhon: a data analysis software for nuclear resonant inelastic X-ray scattering with applications to Fe, Kr, Sn, Eu, and Dy, J. Synchrotron Rad. 25, 1581, 2018.

- Materne P., Bi W., Alp E. E., Zhao J., Hu M. Y., Jesche A., Geibel C., Kappenberger R., Aswartham S., Wurmehl S., Büchner B., Zhang D., Goltz T., Spehling J. & Klauss H. H., Phys. Rev. B. 98, 14517, 2018.

- Ying J., Zhao J., Bi W., Alp E.E., Xiao Y., Chow P. and Struzhkin V.V., Unexpected complex magnetic phase diagram of 𝜺’-FeH, (submitted) 2018.

- Liu J., Wang W., Dauphas N., Yang H., Wu Z., Hu M.Y., Zhao J., Bi W., Alp E.E., Liang W., Chen B., Lin J-F., Carbon isotopic signatures of diamond formation mediated by iron redox chemistry, Geochem. Perp. Let. (submitted) 2018.

- Liu J., Hu Q., Bi W., Yang L., Xiao Y., Chow P., Meng Y., Prakapenka V.B., Mao H-K., Mao W.L., Altered chemistry of O, Fe and H in the middle Earth, Nat. Commun. (under review) 2018.

- List of proposals granted beamtime and usage

Please find the attached excel file titled ”3ID_Users_Statistics_2018”.

- The beamtime schedule for the last year’s cycles

Please refer to the attached excel file titled ”3ID_beam_schedule_2018”.

- List of users in the Mössbauer lab from geosciences and high pressure physics

Community.

| PI | Institution | PI | Institution |
| --- | --- | --- | --- |
| Jay Bass | UIUC | James Walsh | Northwestern U. |
| Anat Shahar | CIW | Ercan Alp | Argonne National Lab |
| Mathieu Roskosz | Muséum National d'Histoire Naturelle | Dam Shim | Arizona State University |
| Jennifer Jackson | Caltech | Marc Hirschmann | U. of Minnesota |
| Susannah Dorfman | Michigan State Univ. | Nicolas Dauphas | U. of Chicago |
| Jung-Fu Lin | Univ. of Texas at Austin | Yanbing Wang | GSECARS, U. of Chicago |
| Kayla Iacovino | ASU |  |  |