Partnership for Extreme Crystallography (PX^2)

2018 COMPRES Annual Report

November 2017 – October 2018

Prepared by Dongzhou Zhang, Przemyslaw Dera, University of Hawaii at Manoa

Overview

Partnership for eXtreme Xtallography (PX^2) is providing new capabilities for high-pressure diamond anvil cell research at the GSECARS APS beamline.  The PX^2 project is a collaboration between the University of Hawaii and GSECARS, supported by COMPRES and hosted by GSECARS at experimental station 13-BM-C.  This beamline provides focused X-rays at two fixed energies: 15 and 28.6 keV and a unique 6-circle heavy duty diffractometer, optimized for a variety of advanced crystallography experiments including interface studies, powder and single crystal structure determination, equation of state studies and thermal diffuse scattering.  Currently we support high pressure and temperature experiments using resistively heated diamond anvil cells, and have achieved P-T conditions of 100 GPa and 1500 K. A new compact optical platform has been installed and provides ruby-fluorescence pressure determination, black-body radiation temperature measurement and Raman spectroscopy capabilities.

The beamline has now a well-established and very active user base. We have been receiving a steady stream of GUP proposals that each cycle well exceed the 50% fraction of beam time for which PX^2 was planned. Since the last annual report the number of published peer-reviewed papers resulting from the PX^2 user program has reached 18, with 1 paper published in the prestigious journal Science, and 1 paper published in Nature Communications.

In 2018 the main technical development thrust was placed on the time-resolved area detector for high pressure single crystal diffraction research. With the help of GSECARS staff Mark Rivers, Peter Eng, Joanne Stubbs and Vitali Prakapenka, several detectors were comprehensively tested and compared, including the Pilatus3, Bruker Photon II, Perkin Elmer and MARCCD. A careful comparison of the detectors suggests that the Pilatus3 1M detector with 1mm Si sensor has the best signal-to-noise ratio and the least background among all tested detectors, and also features a good time resolution (25 frames/sec, 0.002 sec readout time) and a suitable detector area (169 mm X 179 mm).  So we decided to purchase the Pilatus3 1M detector, and the detector is co-funded by COMPRES and GSECARS. The detector arrived in late August of 2018, and has been commissioned at PX^2 in early October. It will be available to general users in the 2019-1 run.

Scientific Highlights

- Valence and spin states of iron are invisible in Earth’s lower mantle (Liu et al., Nature Comm. 2018, 9:1284). Heterogeneity in Earth’s mantle is a record of chemical and dynamic processes over Earth’s history. The geophysical signatures of heterogeneity can only be interpreted with quantitative constraints on effects of major elements, such as iron on physical properties including density, compressibility, and electrical conductivity. However, deconvolution of the effects of multiple valence and spin states of iron in bridgmanite (Bdg), the most abundant mineral in the lower mantle, has been challenging. Here we show through a study of a ferric-iron-only (Mg0.46Fe3+0.53)(Si0.49Fe3+0.51)O3 Bdg that Fe3+ in the octahedral site undergoes a spin transition between 43 and 53 GPa at 300 K. The resolved effects of the spin transition on density, bulk sound velocity, and electrical conductivity are smaller than previous estimations, consistent with the smooth depth profiles from geophysical observations. For likely mantle compositions, the valence state of iron has minor effects on density and sound velocities relative to major cation composition.

Fig 1: Compression behavior of bridgmanite (Bdg) at 300 K across the spin transition. An unit cell volume of (Mg0.46Fe3+ 0.53)(Si0.49Fe3+ 0.51)O3 Bdg and second order Birch–Murnaghan equation of state fits to the high-spin data between 24.7 and 43.1 GPa (dotted) and 50% low-spin data between 52.5 and 61.4 GPa (dashed). Softening is observed between 43.1 and 52.5 GPa (dot dashed). The compression curve of MgSiO3 Bdg is also plotted for comparison (black curve). Inset: normalized stress F vs. Eulerian strain f calculated using the fitted 1-bar unit cell volume from the lower pressure segment, revealing a discontinuity between 43.1 and 52.5 GPa. The error bars are 95% confidence intervals

- High-Pressure 𝛾-CaMgSi2O6: Does Penta-Coordinated Silicon Exist in the Earth’s Mantle? (Hu et al., GRL 2017, 44:11340-11348): Earth is a rocky planet and is dominated by silicates. Crust and upper mantle of our planet feature minerals with silicon almost exclusively in four-coordinated sites, whereas minerals with silicon in six-coordinated sites dominate the transition zone and the lower mantle. It is a long-standing question whether five-coordinated Si phases exist. Five-coordinated Si is observed in silicate glass and melt upon compression as intermediate states and can provide important insight into the transformation mechanism in silica densification. In this paper, we observed a high-pressure crystalline silicate phase with five-coordinated Si. This affects chemical reactivity, elastic and plastic deformation, density of the subducted slab, and its buoyancy relative to the surrounding mantle.

Fig 2: (a) Layer 1 of C2/c 𝛼-diopside phase with IV Si4+. 𝜃 is the O3-O3-O3 angle. Green arrows show the Si-O chain rotation and translation. (b) Layer 2 of C2/c 𝛼-diopside phase with IV Si4+. (c) Layer 1 of P21/c 𝛽-diopside phase with VI Si4+. (d) Layer 2 of P21/c 𝛽-diopside phase with IV Si4+. (e) Layer 1 of P21/c 𝛾-diopside phase with VISi4+. (f ) Layer 2 of P21/c 𝛾-diopside phase with V Si4+. Si and O atoms are represented by grey and red, respectively. Solid black rectangular box is the unit cell. Same color denotes the same Si-O distance in different figures. Magenta solid triangle facets represent O-O-O planes above Si atoms and green solid triangles facets represent O-O-O planes above Si atoms.

- Phase Transitions in Orthoenstatite and Subduction Zone Dynamics: Effects of Water and Transition Metal Ions (Xu et al., JGR-Solid Earth, 2018, 123:2723-2737): Synchrotron-based high-pressure and temperature single-crystal X-ray diffraction experiments were conducted on two hydrous orthoenstatite samples (oEn#1: Mg1.004Si0.996O3, ~619 ppm water; oEn#2: Mg0.947Ni0.055Si0.998O3, ~696 ppm water) to ~34 GPa and 700 K, using resistively heated diamond anvil cells. The α-opx (Pbca space group)→β-opx (P21/c space group) phase transition of oEn#1 occurs at 12.90(2) GPa, and the β-opx phase persists to 34.25(1) GPa. The α-β transition of oEn#2 occurs at 13.50(1) GPa, and a new isosymmetric β-opx→β-opxII transition takes place at 29.80(4) GPa. The β-opxII phase is preserved down to 24.53(3) GPa during decompression. The transition to the monoclinic β-opxII phase is interpreted as a result of incorporation of Ni2+ into the orthoenstatite structure. Fitting the third-order Birch-Murnaghan thermal equation of state to the single-crystal P-V-T data yields the thermoelastic parameters of the α- and β-opx phases for both orthoenstatite samples. This study is the first attempt to determine the thermal equation of state of the β-opx phase. Our results suggest that several hundred ppm of water has negligible effects on the bulk modulus of orthoenstatite but notably enhances the thermal expansion. The potential effects of metastable orthoenstatite on subduction zone dynamics are discussed, and the possible contributions of displacive phase transitions to enhancement of the transformational faulting mechanism of the deep-focus earthquakes in subducted slabs are considered. The presence of metastable orthoenstatite within cold slabs could promote slab stagnation above the 660-km discontinuity.

- The high-pressure anisotropic thermoelastic properties of a potential inner core

Fig 3: Pressure evolutions of normalized unit-cell volume and lattice parameters for (a) oEn#1 and (b) oEn#2. Data collected during decompression are indicated by open symbols. The error bars of the data points are smaller than the symbols.

carbon-bearing phase, Fe7C3, by single-crystal X-ray diffraction (Lai et al., American Mineralogist, 2018, 103:1568-1574). Carbon has been suggested as one of the light elements existing in the Earth’s core. Under core conditions, iron carbide Fe7C3 is likely the first phase to solidify from a Fe-C melt and has thus been considered a potential component of the inner core. The crystal structure of Fe7C3, however, is still under debate, and its thermoelastic properties are not well constrained at high pressures. In this study, we performed synchrotron-based single-crystal X-ray diffraction experiment using an externally heated diamond-anvil cell to determine the crystal structure and thermoelastic properties of Fe7C3 up to 80 GPa and 800 K. Our diffraction data indicate that Fe7C3 adopts an orthorhombic structure under experimentally investigated conditions. The pressure-volume-temperature data for Fe7C3 were fitted by the high-temperature Birch-Murnaghan equation of state, yielding ambient-pressure unit-cell volume V0 = 745.2(2) Å3, bulk modulus K0 = 167(4) GPa, its first pressure derivative K0ʹ = 5.0(2), dK/dT = –0.02(1) GPa/K, and thermal expansion relation aT = 4.7(9) × 10-5 + 3(5) × 10-8 × (T – 300) K-1. We also observed anisotropic elastic responses to changes in pressure and temperature along the different crystallographic directions. Fe7C3 has strong anisotropic compressibilities with the linear moduli Ma > Mc > Mb from zero pressure to core pressures at 300 K, rendering the b axis the most compressible upon compression. The thermal expansion of c3 is approximately four times larger than that of a3 and b3 at 600 and 700 K, implying that the high temperature may significantly influence the elastic anisotropy of Fe7C3. Therefore, the effect of high temperature needs to be considered when using Fe7C3 to explain the anisotropy of the Earth’s inner core.

Fig 4: The P-V-T data of Fe7C3 fitted by the high-temperature Birch-Murnaghan EoS. The pressure and volume uncertainties are within the symbols. Solid curves are the fitting results.

Beamline Personnel

Project PI: Przemyslaw Dera (University of Hawaii at Manoa)

Przemek is the PI of the PX^2 project.

Beamline scientist: Dongzhou Zhang (University of Hawaii at Manoa)

Dongzhou is the beamline scientist of the PX^2 project. He is responsible for the user support of PX^2. Dongzhou is fully supported by COMPRES.

Beamline student intern: Yi Hu (University of Hawaii at Manoa)

Yi has served as the beamline student intern since 2016. Her responsibilities included completion of the portable ruby system and limited user support.

Related personnel:

Peter Eng (GSECARS, University of Chicago)

Peter is the beamline scientist of GSECARS in charge of the surface diffraction program of 13BMC. He is involved in the beamline operations and beamline upgrade of the PX^2 program.

Joanne Stubbs (GSECARS, University of Chicago)

Joanne is the beamline scientist of GSECARS in charge of the surface diffraction program of 13BMC. She is involved in the beamline operations and beamline upgrade of the PX^2 program.

Vitali Prakapenka (GSECARS, University of Chicago)

Vitali is the beamline scientist of GSECARS in charge of the diamond anvil cell program. He is involved in the beamline operations and beamline upgrade of the PX^2 program

Mark Rivers (GSECARS, University of Chicago)

Mark is the co-director of GSECARS. He is involved in the beamline upgrade of the PX^2 program.

Beamline Operations

PX^2 is running in a steadfast way in 2018. In each run we receive ~30 GUP requests and host ~25 of them. We allocate ~140 shifts for the GUP users per run. We collaborate closely with other COMPRES supported facilities located at the APS: most of the high pressure DACs measured at PX^2 were gas-loaded at the GSECARS/COMPRES gas loading system; we’ve collaborated with the COMPRES-supported nuclear resonant scattering program (3-ID at the APS), and 4 papers published in 2018 involve both PX^2 and 3-ID experiments. A brief statistics of the user operation is listed below:

Number of beamtime proposals received: 99

Number of beamtime proposals granted beamtime: 75

Total number of shifts requested: 716

Total number of shifts granted: 419

Total number of shifts available: 438

Oversubscription rate (= shifts requested / shifts available): 1.63

Number of visits by distinct research groups: 64

Number of unique users, categorized by affiliation (University, Gov’t Lab/agency, Private institution, or Industry) and by origin (USA, Canada, Europe, Asia, Other)

Affiliation:

University: 30

Government Lab/agency: 34

Origin:

USA: 24

Canada: 1

Asia: 39

Total number of person-visits: 75

Number of undergraduate users: 0

Number of graduate student users: 16

Number of visits funded by each funding agency (NSF, DOD, DOE, Foreign/Other)

NSF: 27

DOE: 6

NNSA: 2

NASA:1

University: 4

NSERC: 1

Foreign: 39

Shifts are counted for PX^2 GUP experiments only (excluding the surface diffraction program at 13-BM-C). Details of the successful proposals, beamtime allocated, and total usage is provided in Appendix I.

Performance Metrics

One spreadsheet (Appendix I) is attached for PX^2 user statistics for the year of 2018. PI name, country, funding source, and beamtime allocation of all PX^2 GUPs and in-house setup beamtimes are listed. All COMPRES users at PX^2 get their beamtime through the APS GUP system. In the year of 2018, 27 GUP beamtime requests were made from COMPRES members, and 156 shifts were allocated to COMPRES members.

Beamline Community Activities

1. PX^2 co-organized the 2018 Workshop of the IUCr Commission on High Pressure, held in Honolulu, HI, July 29 - August 2. 108 researchers from 16 countries attended the workshop, and 52 oral and 36 poster presentations were given during the conference. The workshop aimed to bring together scientists studying crystallography of extreme materials and extreme phenomena under extreme environments. PX^2 PI, Przemek Dera served as the chair of the workshop, and Dongzhou Zhang served as an organizing committee member. COMPRES financially supported the workshop through an EO&ID grant, and the support was leveraged by other institutions including University of Hawaii, GSECARS, HPCAT and industrial partners. NSF also allocated an additional grant (EAR-1834441) to cover the participation cost of 10 US-based young scientists, with Dera and Zhang as PIs.

A one-day satellite crystallographic training session was held on July 28 at the University of Hawaii campus, which was attended by 48 participants. The training session aimed to teach graduate students and junior researchers to analyze the single crystal diffraction data. Zhang offered lecture as part of the training session. COMPRES Beamline Scientist Christine Beavers from ALS 12.2.2, also gave lectures, both in the training session, and during the main conference event. COMPRES supported the training session as part of the EO&ID grant, and participation in this activity was offered to the conference attendees for free.

Figure 5: Participants of the 2018 workshop of the IUCr Commission on High Pressure in Honolulu, HI.

Figure 6: Data analysis software training session at the 2018 workshop of the IUCr Commission on High Pressure in Honolulu, HI.

2. Since Run 2018-2, PX^2 beamline scientist Dongzhou Zhang has been serving at the APS high pressure proposal review panel. This panel reviews scattering and diffraction proposals that focus on materials at high pressure among all APS beamlines.

Beamline Development

The major development of PX^2 in the current fiscal year has been the upgrade of X-ray area detector. Area detector is one of the most essential instrument components for X-ray diffraction studies. PX^2 has been using a 15-year old MAR165 CCD detector, with readout rate of 0.3 frames, which has been the efficiency bottleneck of single crystal diffraction at PX^2. In single crystal experiments the data is acquired in a series of steps that cover a gradual rotation of the sample. With slow readout detector this process cannot be accomplished continuously, but the data acquisition has to be stopped after each step to avoid data loss. In the past few years, we also experienced technical problems with this aging detector (loss of vacuum), which affected the user operations. The plan to purchase a new state-of-the-art detector for the beamline was included in the COMPRES renewal proposal. COMPRES agreed to fund the detector in late 2017. In an effort to select the best available technology, several different detectors were evaluated at PX^2 between 2017 and 2018, including Bruker Photon II, Perkin Elmer, and Pilatus. After careful comparison of the test data, we concluded that the Pilatus 1M detector with 1 mm Si is the most suitable detector to meet our requirements. The Pilatus 1M detector features a photon counting mechanism (hence nearly zero background), and has a fast, 25 frames/sec readout rate. The Pilatus detector purchase was co-funded by COMPRES and GSECARS, and has been commissioned in October 2018. The upgrade to Pilatus 1M detector will give PX^2 the capability to carry out continuous on-the-fly diffraction on single crystals, and will significantly reduce the data collection time (up to 2 orders of magnitude). We have developed a protocol to collect single crystal data in a continuous way, and a workflow to process the Pilatus data using the Bruker APEX 3 software package.

Figure 7: Left: The new Pilatus3S 1M Si detector being commissioned at PX^2. Right: Carl Agee, President of COMPRES and Mark Rivers, GSECARS Co-Director, inspect the new Pilatus 3S 1M Si detector at PX^2 (September 28, 2018).

Figure 8: Screenshot of Bruker APEX 3 software while processing diffraction data taken with the Pilatus 1M Si detector. The sample is a NIST-calibrated LaB6 crystal.

Table 1: Comparison of the data collection time and storage efficiency between the old MAR165 CCD and the new Pilatus 3S detector.

| Detector | MAR165 CCD | Pilatus3S |
| --- | --- | --- |
| Typical measurement condition | 70 degrees opening diamond anvil cell and 1 detector position |  |
| Total number of images | 70 (thin segments) + 7 (wide segments), tiff image | 70 (continuous fly scan), cbf image |
| Experimental time | Typical exposure time: 1s/deg CCD readout time: 2.5s Back-rotation overhead: 2.5 s 70*(1s+2.5s+2.5s) + 7*(10s+2.5s+2.5s) = 525 s | Typical exposure time: 0.1s/deg 70*0.1s = 7 s |
| Hard drive space | 77 * 8196 kB = 631 MB | 70 * 1006 kB = 70.4 MB |

Planned Activities

In the next year, PX^2 will work on combining laser heating, time-resolved detector and high pressure single crystal diffraction, so as to carry out crystallographic research under the earth’s lower mantle and core conditions. So far, in-situ laser heated single crystal diffraction at high pressure has been achieved only in a handful of cases. At PX^2, the 200W IR laser heating system has been commissioned to carry out laser-heated diffraction at ambient pressure, and high pressure heat-and-quench diffraction in diamond anvil cells. For in-situ experiments, the time-resolved Pilatus detector is necessary, because the fast on-the-fly data collection significantly reduces the uncertainty in temperature determination and improves the successful rate of experiments. The high pressure single crystal diffraction with in-situ laser heating will be achieved by introducing new designs of diamond anvil cells. In-situ laser heated high pressure single crystal diffraction with round-table diamond anvil cell has been prototyped in 13-ID-D, and we are working on refining this technique, and incorporating it in the current PX^2 setup.

Figure 9: Preliminary test of laser-heated in-situ single crystal diffraction at ambient pressure. Left: image of the Pt single crystal during the single crystal diffraction experiment. The crystal was made by melting and re-crystallization of tip of a Pt wire. Right: diffraction pattern of the Pt single crystal at ~1950 K. The diffraction image was collected by a MAR165 CCD in 3 minutes. It is worth mentioning that at high pressures, the sample will not be in a perfect spherical shape, and the temperature will fluctuate during rotation (required by single crystal diffraction). Therefore, a time-resolved area detector is imperative to reduce the uncertainty of temperature for in-situ high pressure single crystal diffraction experiment.

Personnel

PX^2 program operation was originally planned for one beamline scientist to support up to 50% of the available beam time, with the other half of the time to be used by the surface scattering program. Since PX^2 opened for user operation in 2015, the demand for beam time increased rapidly, and currently the high pressure program at 13BM-C operates for almost 80% of time each run. With significant commissioning activities continuing (e.g. implementation of new time-resolved detector), the workload far exceeded one FTE, and in FY2018 COMPRES approved recruitment of second, Jr. Beamline Scientist. Because in 2018 the beamline intern, Yi Hu, was still available to support the PX^2 program, recruitment of the Jr. Beamline Scientist was scheduled for the fall of 2018. Yi Hu defended her Ph.D. thesis at the University of Hawaii in October 2018 and secured a new position with Canon Medical Research, Inc. The job opening for the Jr. Beamline Scientist position has been advertised through the COMPRES, MSA and AIRAPT mailing lists. 9 eligible applications have been received, of which 5 candidates have been scheduled for Skype interviews in the second part of November. The Search Committee anticipates starting the new position in January 2019.

2019-2020 Budget justification

The overall budget request for FY 2019 is for $254,210, which is a modest, 4% increase, compared to FY 2018 budget.

1. Personnel

The PX^2 Sr. Beamline Scientist‘s projected salary for 2018 is $76,874. The anticipated inflation-based increase of base salary is 3% annually.

The budget includes funds to support a second full time Junior Beamline Scientist to accommodate dramatically increased number of users supported by the facility and  fraction of total beam time at 13BM-C used by the PX^2 program. The PX^2 Jr. Beamline Scientist‘s position is expected to be filled in January 2019. Projected base salary for this position in 2019 is $55,000.

Commissioning and instrument improvement activities will continue at PX^2 through the whole COMPRES IV period. We would like to continue the arrangement with the discounted services of single SOEST engineer, Harold Garbeil, whose primary competences are in 3d design, electrical engineering, and software development. The cost of this engineering support is calculated based on a discounted monthly 1.0 FTE salary of $ $10,373 and 1 calendar month of effort per year. Engineering support will be particularly critical in further commissioning of the new area detector and its full integration within the data acquisition and analysis framework.

2. Fringe Benefits

Fringe benefits for the Beamline Scientist are calculated based on the RCUH rate of 38.2%. Fringe benefits for the engineering staff are calculated at 61.56%.

3. Travel Expenses

The PI anticipates requiring travel expense support for the PX^2-related activities at Argonne one trip a year, with estimated cost of the trip at $3,000. For the PX^2 Beamline Scientist and Junior Beamline Scientist we request funds to travel to the COMPRES Annual Meeting or the AGU Annual meeting. Estimated cost of each trips is $2,000 and one such trip is budgeted for 2018.

4. Materials and Supplies

Chemicals, heating wires, gaskets, materials for custom parts machining		$1,000

Electronic components 								$1,000

Any DAC experiments will require supplies such as commercially available chemicals as samples or substrates for sample synthesis, solvents, rhenium gaskets for diamond anvil cells, raw materials for machining of custom parts and adapters, etc. The facility commonly makes these materials available to users. A budget of $1K is requested for these purposes.

PX^2 is a very complex hardware installation featuring over a hundred different motors, detectors of various type and signal processing electronics. These components ware out with time and require updates/upgrades to maintain the state-of-the art. The beamline operation also relies on a variety of software, some of which is commercial. A budget of $1,000 is requested for these purposes.

5. Indirect Costs

Indirect costs are calculated based on the University of Hawaii approved off-campus rate of 24%.

Appendices

1. A publication list for 2017 and 2018. Include peer-reviewed publications and theses, but not conference abstracts.

2. A list of proposals granted beamtime and usage (PI, Affiliation, Title, Funding, Days requested / Days allocated / Days used, etc.) for each of the last year’s cycles for each beamline or side station.

3. The beamtime schedule for the last year’s cycles.

4. Copies of all End of Experiment questionnaires from PX^2 users are included is a separate file.