Partnership for Extreme Crystallography (PX^2)

2016 COMPRES Annual Report

November 2015 – October 2016

Prepared by Dongzhou Zhang, Przemyslaw Dera, University of Hawaii at Manoa

Overview

Partnership for eXtreme Xtallography (PX^2) is providing new capabilities for high-pressure diamond anvil cell research at the GSECARS APS beamline.  The PX^2 project is a collaboration between the University of Hawaii and GSECARS, supported by COMPRES and hosted by GSECARS at experimental station 13-BM-C.  This beamline provides focused x-rays at two fixed energies: 15 and 28.6 keV and a unique 6-circle heavy duty diffractometer, optimized for a variety of advanced crystallography experiments including interface studies, powder and single crystal structure determination, equation of state studies and thermal diffuse scattering.  Currently we support high pressure and temperature experiments using resistively heated diamond anvil cells, and have achieved P-T conditions of 100 GPa and 1500 K. A new compact optical platform has been installed and provides ruby-fluorescence pressure determination, black-body radiation temperature measurement and Raman spectroscopy capabilities.  These new capabilities are available to all researchers interested in studying deep earth materials through the APS General User Proposal system.

Experimental instruments

- 50% beamtime, sharing with surface diffraction program of GSECARS

- X-ray energy of 15/28.6 keV, focused to 15×15 micron2

- Monochromized X-ray with eV bandwidth

- 6-circle kappa geometry diffractometer

- Area detector (MAR165 CCD, Pilatus 100K)

- Resistive heating setup, including power supply, thermal couple temperature reading and water cooling

- Compact optical platform capable of doing ruby-fluorescence pressure determination, black-body radiation temperature reading and Raman spectroscopy measurements

Personnel

Project PI: Przemyslaw Dera (University of Hawaii at Manoa)

Przemek serves the PI and coordinator of the PX^2 project.

Beamline scientist: Dongzhou Zhang (University of Hawaii at Manoa)

Dongzhou is the beamline scientist of the PX^2 project. He is responsible for the user support of PX^2. Dongzhou has been working in PX^2 since Jan 2015, and is fully supported by COMPRES.

Related personnel:

Peter Eng (GSECARS, University of Chicago)

Peter is the beamline scientist of GSECARS in charge of the surface diffraction program of 13BMC. He is involved in the beamline operations and beamline upgrade of the PX^2 program.

Joanne Stubbs (GSECARS, University of Chicago)

Joanne is the beamline scientist of GSECARS in charge of the surface diffraction program of 13BMC. She is involved in the beamline operations and beamline upgrade of the PX^2 program.

Vitali Prakapenka (GSECARS, University of Chicago)

Vitali is the beamline scientist of GSECARS in charge of the diamond anvil cell program. He is involved in the beamline operations and beamline upgrade of the PX^2 program

Mark Rivers (GSECARS, University of Chicago)

Mark is the co-director of GSECARS. He is involved in the beamline upgrade of the PX^2 program.

List of users and affiliations, 2015-2016

Yi Hu, Hannah Shelton, Jin S. Zhang, Jingui Xu, Xiaojing Lai, Bin Chen (University of Hawaii at Manoa); John Lazarz, Fei Qin, Xiaobing Liu (Northwestern U); Wenge Yang, Gang Liu, Lingping Kong, Qingyang Hu, Liuxiang Yang (Carnegie Institution of Washington); Shuai Zhang (UC Berkeley); Jiuhua Chen, Fei Han (FIU); Spencer Smith (U Alabama); Sean Shieh (U Western Ontario); Feng Zhu, Junjie Dong (U Michigan); Jiachao Liu (Michigan State U); Lu Ma (Ohio State); Xiangyi Luo (ANL); Yuejian Wang (Oakland U); Yahya Al khatatbeh (Yale); Arthur Liu (Harbin Inst. Tech); Fuyang Liu, Su-Ying Chien, Shengyi Xie, Mingqiang Hou (HPSTAR)

Details of beamtime allocation are listed in Appendix I.

Publications and products, 2015-2016

- Synthesis of FeO2 and the Fe-O-H system in the deep Earth (Hu et al., Nature, 531, 241-244 (2016), highlighted by COMPRES website). The Earth’s geochemistry can be regarded as a ternary system of oxygen, its most abundant element by atomic fraction, iron, its major redox ingredient, and hydrogen, its most mobile element responsible for electron transfer. The oxygen rich atmosphere and iron rich earth core represent the two end members of the O-Fe system, overlapping the entire pressure-temperature (P-T) range of the planet. We explored the chemical reaction in the system of Fe-O-H at high-pressure and high-temperature that mimics deep lower mantle (DLM) conditions. When hematite is compressed in O2 and heated above 76 GPa and 1800 K, a new FeO2 phase is identified through X-ray diffraction conducted at synchrotron beamlines, including the Partnership for Extreme Crystallography at Advanced Photon Source, Argonne National Laboratory. The spotty FeO2 diffraction pattern was solved by the so-called multigrain crystallographic method. The newly discovered FeO2 phase holds an excessive amount of oxygen and has the same atomic structure as FeS2. We went on to show that the mineral goethite (FeOOH) can also decompose to FeO2 at 92 GPa and 2050 K by releasing hydrogen. In DLM situation, the hydrogen released from FeOOH would diffuse, infiltrate or react to form hydrocarbon or other volatiles. At the same time, FeO2 patches are left in DLM and cumulate through plate tectonics. Such process provides an alternative interpretation to the origin of seismic and many geochemical signatures in the DLM.

- Band-gap narrowing together with carrier-lifetime prolongation in perovskite-structured compound (Kong et al., PNAS, 113 (32), 8910-8915 (2016)). Hybrid perovskites are believed to be among the most promising materials for the next generation of solar cells. The solar cells convert solar energy into electrical energy so it's a sustainable and environmentally friendly energy source, giving high performance at a low cost. In addition to solar cell technologies, the hybrid perovskites have potential to be used in a variety of optoelectronic applications. Its power-conversion efficiency has been increased to 22.1% at present. High absorption for solar energy and photovoltage for longing the carrier-lifetime in hybride perovskites are key factors for their actual usage in energy science.

- Compressional behavior of omphacite (Zhang et al., PCM, 43(10), 1-9 (2016)). Omphacite is an important mineral component of eclogite. Single crystal synchrotron X-ray diffraction data on natural (Ca,Na)(Mg,Fe,Al)Si2O6 omphacite have been collected up to 47 GPa at ambient temperature. Unit cell parameter and crystal structure refinements were carried out to constrain the isothermal equation of state and compression mechanism. The elastic parameters are consistent with the general trend of the diopside-jadeite join. The eight-coordinated polyhedra are the most compressible, and contribute to majority of the unit cell compression, while the SiO4 tetrahedra behave as rigid structural units and are the most incompressible. Axial compressibilities are determined by fitting linearized BM3 equation of state to pressure dependences of unit cell parameters. Throughout the investigated pressure range, the b-axis is more compressible than the c-axis. The axial compressibility of the a-axis is the largest among the three axes at 0 GPa, yet it quickly drops to the smallest at pressures above 5 GPa, which is explained by the rotation of the stiffest major compression axis toward the a-axis with the increase of pressure.

- Isosymmetric pressure-induced bonding increase changes compression behavior of clinopyroxenes across jadeite-aegirine solid solution in subduction zones (Xu et al., JGR-Solid Earth, in press). Synchrotron-based single-crystal X-ray diffraction experiments were carried out on a natural aegirine [NaFe3+Si2O6] sample at ambient temperature and pressures to 60 GPa, simulating conditions within the coldest part of a subduction zone consisting of old lithosphere. The diffraction data reveal no obvious sign of structural phase transition in aegirine within this pressure range, however several relevant structural parameter trends change noticeably at approximately 24 GPa, indicating presence of the previously predicted isosymmetric bonding change, related to increase of coordination number of Na+ at M2 site. The pressure-volume data, fit with 3rd order Birch-Murnaghan(BM3) equation of state over the whole pressure range, yields KT0 = 126(2) GPa and K′T0 = 3.3(1), while separate BM3 fits performed for the 0-24.0GPa, and 29.9-60.4 GPa pressure ranges give KT0=118(3), K’T0= 4.2(3) and KT0 = 133(2), K′T0=3.0(1), suggesting that the structure stiffens as a result of the new bond formation. Aegirine exhibits strong anisotropic compression with unit strain axial ratios ε1:ε2:ε3=1.00:2.44:1.64. Structural refinements reveal that NaO8 polyhedron is the most compressible, and SiO4 tetrahedron has the lowest compressibility. The consequence of bonding transition is that the compressional behavior of aegirine below ~24 GPa and above that pressure is quite different, with likely consequences for relevant thermodynamic parameters and ion diffusion coefficients.

- Metastable augite at high pressure and temperature conditions and its implications for subduction zone dynamics (Xu et al., Am. Min., in revision). We present the synchrotron-based single-crystal X-ray diffraction study on a natural diopside-dominated augite at high pressures and temperatures to ~27 GPa and 700 K to simulate conditions within the cold subducting slabs. Our results indicate that augite is stable over this pressure and temperature range. The third order high-temperature Birch–Murnaghan equation was used to fit the pressure-volume-temperature data and yields the thermoelastic parameters. The strain analysis is conducted and the results show that the compression along the three principal stress directions is highly anisotropic with ε1:ε2:ε3=1.98:2.43:1.00. Additionally, high-pressure structural refinements of polyhedral geometry, bond lengths and O3-O3-O3 angle were investigated to ~27 GPa at ambient temperature. Pressure dependences of polyhedral volumes and distortion indicate that the incorporation of Al3+ in the T site would significantly changes the compression behavior of the T-tetrahedron in augite.

- High pressure equation of state of magnesiowüstite (Finkelstein et al., under review). Magnesiowüstite, (Mg,Fe)O, solid solutions with high iron enrichment may be an important component of ultra-low velocity zones at Earth’s core-mantle boundary. However, to date there have been few high-precision studies on the elastic properties of these materials. In this study we present results on the compression of (Mg0.22Fe0.78)O (Mw78) in both neon and helium pressure media using single-crystal diffraction to ~55 GPa. In addition, our sample was characterized by time domain synchrotron Mössbauer spectroscopy at ambient pressure using an extended time range that resulted in vastly improved energy resolution. We make two main observations: K0T decreases as a function of increasing iron content and K'0T remains at approximately 4.0 independent of iron content. In combination with previously reported thermal parameters, we extrapolate elastic parameters of Mw78 to deep-Earth conditions and determine estimated density profiles.

Beamline Operations

In the fiscal year of 2016, APS had in total 625 shifts (5000 hours) available for experiments. PX^2 shares half of the shifts available (312 shifts) with the surface diffraction program at GSECARS. Among the 312 shifts available, about 10% was used for commissioning experiments and setup switch between PX^2 and the surface diffraction program. GSECARS kindly made available to  PX^2 several essential components, including the experimental hutch, 6-circle diffractometer, power supplies and digital multimeter for resistive heating setup, gas loading system and the offline sample preparation lab.

Number of beamtime proposals received: 45

Number of beamtime proposals granted beamtime: 41

Total number of shifts requested: 390

Total number of shifts granted: 278

Total number of shifts available: 312

Oversubscription rate (= shifts requested / shifts available): 1.25

Number of visits by distinct research groups: 23

Number of unique users, categorized by affiliation

University: 15

National Lab/public agency: 4

Private institution: 4

Number of unique users, categorized by origin:

USA: 17

China: 5

Canada: 1

Total number of person-visits: 41

Number of undergraduate users: 0

Number of graduate student users: 7

Number of visits funded by each funding agency

NSF: 20

DOE: 11

Foreign: 12

Details of the successful proposals, beamtime allocated, and total usage is provided in the attachment.

Performance Metrics

General User Time for COMPRES: For higher-ranked proposals with beamtime allocated by the facility: 215 shifts was granted to users COMPRES members and foreign affiliates in the year of 2016 (77.3% of total beamtime granted), and 197 shifts was granted to users from domestic COMPRES institutions (70.9% of total beamtime granted).

Contributing User Time: Allocated for COMPRES users who were not assigned GU time: we have not had any contributing user time in the year of 2016.

Total time for COMPRES users (there will usually be GU and CU COMPRES users): 197 shifts.

Recent upgrades of the beamline

- Compact optical platform for ruby pressure determination and Raman spectroscopy: Pressure determination is important for diamond anvil cell experiments. Currently, the most convenient method to determine the pressure in the sample chamber is ruby fluorescence. A compact optical platform to the 13-BM-C station was installed in early 2016, which is capable of determining pressure with ruby fluorescence, as well as collecting Raman spectra on the sample. This compact optical platform has been appreciated by the users. With this platform, the users can easily control the pressure of their diamond anvil cells with membrane pressure controller.

- Resistive heating and temperature readout setup: Contemporary research on Earth-related materials requires not only high pressure, but also high temperature, and resistive-heated diamond anvil cell has been broadly used in recent mineralogy experiments. The remotely-controllable resistive-heating and temperature reading setup has been upgraded in the experimental station 13-BM-C. With the support from COMPRES, a new 1000-W power supply has been purchased to power the heaters in the DACs, and a new thermal couple reader has been installed, which provides a faster temperature readout rate and requires less computational resource than the old Keithley-type digital multimeter. The setup is capable of heating the samples up to 1000 C, and has been used by the users since the run of 2016-2.

- Membrane pressure controller update: Diamond anvil cells mounted in membrane pressure controller allows pressure to be changed remotely, and is therefore more convenient for user operations. In early 2016, the membrane pressure controller was installed in 13-BM-C, with automatic remote control capability. This setup significantly reduces the time needed for the users to change the pressure of their sample, and is appreciated by the users. The membrane pressure controller is working synergistically with the resistive-heating setup and the compact optical table. In one of our test, the users can control the data collection process remotely from the University of Hawaii’s campus in Honolulu.

- X-ray instrumentation: In diamond anvil cell experiments, most of the experimenters use X-ray pin-diode to scan and align the sample’s position. In the past, the X-ray pin-diode in 13-BM-C was bulky, pneumatically-driven, moving in-and-out during the measurement, which caused significant instability to the other components. The old X-ray pin-diode was replaced with a new compact pin-diode incorporated into the X-ray beamstop. This integrated pin-diode beamstop provides additional stability to the diffractometer.

- Software development: In the mid-2016, with the help of Dr. Jesse Smith from HPCAT, the single crystal diffraction data collection software was upgraded in 13-BM-C. This new software is based on Python, rather than the old IDL 6.4 program, and it provides a better time synchronization between the X-ray shutter and the X-ray detector.

Community development and outreach activities

- Beamline Scientist Dongzhou Zhang was invited to give a talk in the 2015 AGU Fall Meeting in San Francisco, California. Dongzhou presented a poster about the development of the PX^2 program. During this conference, Dongzhou also attended the COMPRES townhall meeting and gave a talk about the future development of PX^2. Besides, Dongzhou received the 2015 MRP Graduate Research Award.

- In January 2016, Beamline Scientist Dongzhou Zhang visited the HPSTAR center in Beijing, China, and gave a talk about the development of the PX^2 program. HPSTAR is one of the biggest high pressure research centers in Asia. Several people in the audience later became visiting scholars to COMPRES member institutions, including the Geophysical Lab and Florida International University, and they carried out experiments at PX^2.

- In May 2016, Beamline Scientist Dongzhou Zhang attended the APS user meeting in Argonne, Illinois. Dongzhou gave a poster about the research development of PX^2 program.

- In June 2016, Beamline Scientist Dongzhou Zhang attended the COMPRES Annual Meeting in Tamaya, New Mexico. Dongzhou was invited to give a talk about the development of PX^2 program. In addition, Dongzhou gave a poster to show the progress of the beamline development.

- In June 2016, Beamline Scientist Dongzhou Zhang attended the 49th International School of Crystallography in Erice, Italy. Dongzhou presented a poster about the development of the PX^2 program. Several attendees of this summer school, including researchers from the University of Utah and Stanford University, later applied to carry out research at the PX^2.

- In October 2016, PI Przemyslaw Dera and Beamline Scientist Dongzhou Zhang attended the high pressure multigrain diffraction workshop organized by HPCAT, and co-chaired by Dera. Przemyslaw and Dongzhou presented talks about the experimental capabilities at the PX^2.

Leverage of COMPRES funding

APS

APS contributed to the PX^2 project by covering the cost of Si 311 monochromator crystal manufacturing. Estimated cost of this expense was $50K. The monochromator was installed in the fall 2014 and enabled the 29 keV incident beam energy capability which was critical for diamond anvil cell studies. Additionally, APS allocated a dedicated laser spectroscopy lab for the needs of the PX^2 project without a cost to COMPRES. This laser lab is located in the APS building 400, and has been extensively used for testing and commissioning of the sample viewing and spectroscopy system for PX^2.

GSECARS

GSECARS equipment contributions to the project include access to the experimental station, the 6-circle Newport diffractometer with motion control infrastructure and access to GSECARS area detectors (MAR165 CCD, MAR345 IP, Perkin Elmer flat panel detector, PILATUS 1K). GSECARS also provides office space for PX^2/UH (currently 3 desks) and computer/networking services at no charge.

Significant portion of the PX^2 instrumentation design, construction and commissioning activities  to date have been supported by GSECASR staff, including Mark Rivers, Peter Eng, Joanne Stubbs, Patric Dell and Mike Proskey. Since September 2013 GSECARS has contributed towards PX^2 significant fraction of effort of these staff members, without any cost to COMPRES:

1. An estimated three months of effort of design drafter, Patrick Dell, who prepared a 3 dimensional model of the 13BM-C instrument and integrated the DAC specific solutions.

2. An estimated one month efforts of Senior Scientist Dr. Peter Eng and Beamline Scientist Joanne Stubbs have been contributed towards upgrade, modification, optimization and testing of the monochromator and focusing optics to adapt them to the diamond anvil cell research requirements.

3. An estimated two weeks effort of GSECARS Director, Dr. Mark Rivers has been contributed towards setting up instrument control software and laser interlock hardware for the new PX^2 XPS motion controller.

4. An estimated two weeks of effort of Mechanical Support Technician Mike Proskey has been contributed towards assembling the new optical platform system for PX^2.

UH

University of Hawaii contributes the project management services of the PI without any summer salary support. During the current fiscal year two trips of the PI to the APS to work specifically on the PX^2 project were covered from the PI UH startup account. The PI provides on-site data analysis training to many PX^2 users.

UH also contributes to the project by providing SOEST mechanical engineering support at the 50% discounted rate.

UH-funded visiting intern graduate student, Jingui Xu has been helping the PX^2 beamline scientist during the commissioning activities in 2016 at no cost to COMPRES.

Summary of budget expenditures for 11/16/2015 – 10/31/2016

[PX^2 + COMTECH ]

Salaries, wages and overload 					$117,801

Dongzhou Zhang, PX^2 beamline scientist

11/16/15-10/31/16 	1.0 FTE x 11.5 months

Mario Williamson, SOEST Engineering Support

11/16/15-10/31/16 	0.1 FTE x 11.5 months

Jin Zhang , COMPTECH Technology Officer

11/16/15-7/15/16 		1.0 FTE x 8.0 months

Yi Hu, COMPTECH intern

6/1/16-10/31/16 		1.0 FTE x 5.0 months

Fringe benefits							$26,933

Materials and supplies 						$23,365

Capital equipment 						$10,469

Navitar motorized zoom system for COMPTECH portable ruby spectrometer

Domestic travel 							$10,864

International travel 						$3,172

Dongzhou Zhang trip to China

Dongzhou Zhang Erice Crystallography School in Italy

Publication costs 						$4,359

Publication fees for audiovisual paper about PX^2 in JoVE

Other 								$5,971

Shipping charges

CNC machining fees

Engineering materials

Outside-UH machining fees (surface grinding, heat treatment)

Total direct costs						$202,933

Indirect costs							$45,542

Total costs							$248,476

Budget for 6/1/2017-5/31/2018 (as submitted for COMPRES renewal)

Budget justification for 6/1/2017-5/31/2018 (as submitted for COMPRES renewal)

- OTHER PERSONNEL

The PX^2 Beamline Scientist‘s projected salary for 2017 is $72.461K. The anticipated inflation-based increase of base salary is 3% annually.

Engineering support:

Commissioning and instrument improvement activities will continue at PX^2 through the whole COMPRES IV period. We would like to continue the arrangement with the discounted services of single SOEST mechanical engineer, M. Williamson (half of the support that was required during the initial intensive commissioning of the program). The cost of this support is calculated based on a discounted monthly 1.0 FTE salary of $ $7,374 and 0.1 FTE per month. The anticipated inflation-based increase of base salary is 5% annually.

- FRINGE BENEFITS

Fringe benefits for the Beamline Scientist are calculated based on the University of Hawaii at Manoa rate of 50.79%. Fringe benefits for the engineering staff are calculated at 29.11%.

- TRAVEL EXPENSES

The PI anticipates requiring travel expense support for the PX^2-related activities at Argonne 2 times a year, with estimated cost of each trip at $2,500.

For the PX^2 Beamline Scientist we request funds to travel to the COMPRES Annual Meeting and the AGU Annual meeting. Estimated cost of each trips are $1,500 and $2000, respectively.

- OTHER DIRECT COSTS

Materials and Supplies

One of the major expenses in high-pressure experiments is the cost of diamond anvils (~$1K/piece). During 2015 PX^2 acquired a stock of 10 anvils. Funds are requested to maintain this stock, perform necessary repairs of damaged anvils, or replace the anvils that are completely broken.

Any DAC experiments will require supplies such as commercially available chemicals as samples or substrates for sample synthesis, solvents, rhenium gaskets for diamond anvil cells, raw materials for machining of custom parts and adapters, etc. The facility commonly makes these materials available to users.

PX^2 is a very complex hardware installation featuring over a hundred different motors, detectors of various type and signal processing electronics. These components ware out with time and require updates/upgrades to maintain the state-of-the art. The beamline operation also relies on a variety of software, some of which is commercial. Funds are requested for these purposes.

- INDIRECT COSTS

Indirect costs are calculated based on the University of Hawaii approved off-campus rate of 24%.

L. AMMOUNT OF THIS REQUEST

$165,425