Diamond-Anvil Cell Infrared Facility at the National Synchrotron Light Source II

2018 COMPRES Annual Report

November 2017 – October 2018

Prepared by Zhenxian Liu and Russell J. Hemley

The George Washington University

Overview

The Frontier Synchrotron Infrared Spectroscopy Beamline under Extreme Conditions (FIS), the successor of NSLS-U2A, is one of the first synchrotron infrared (IR) beamlines on the NSLS-II experimental floor and a new home for the high-pressure infrared user community. With over $2M in funding from the NSLS-II FY16 operational budget, the construction of both the FIS/MET beamline cabins and the end station set-up have been completed. The dipole vacuum chamber and UHV optical extraction system have been manufactured, delivered, and successfully installed during the NSLS-II August-September storage ring shutdown. The ongoing beamline commissioning is going very well and the synchrotron IR beam profile observed at the exit of the UHV optical extraction system is in a good agreement with the calculated one. Final installation of the beam delivery pipe system to the end stations is under way with subsequent science commissioning in December 2018 and operation for general users starting in early 2019. FIS/MET has adapted one of the novel design features of NSLS II – the large-gap IR dipole – to provide unparalleled brightness and more than an order of magnitude greater flux compared to U2A throughout much of the IR spectrum. It will also have improved far-IR capabilities that will continue to enable the high-pressure synchrotron IR program at NSLS to be unique. The source will also have exceptional stability, critical for spectroscopic studies under extreme conditions, such as static and dynamic compression and variable temperatures. Full synchrotron IR capacity is expected in early 2019 that will provide diffraction-limited performance in the entire IR spectral region. FIS is thus not only the successor to NSLS-U2A but also brings the dedicated facility to a new level for optical spectroscopic studies under extreme P-T conditions. The integrated optical facility for far-IR to UV absorption and reflectance spectroscopy with synchrotron and conventional sources, together with laser Raman and photoluminescence spectroscopy, will be available to users for experiments starting in early 2019. Moreover, FIS provides basic infrastructure, such as a non-laser portable ruby system for pressure calibration, a micro-Raman system and a sample preparation workstation, for all high-pressure experiments at NSLS-II and is playing critical role in exploring high-pressure DAC opportunities at other NSLS-II x-ray beamlines for the COMPRES user community.

As a new state-of-art integrated synchrotron IR facility, FIS will be a COMPRES showcase for the earth science and high-pressure research communities worldwide and a unique resource for the COMPRES user community. With the implementation of new developments and upgrades, the facility will allow for a wide range of micro-spectroscopic studies at a broad range of pressures (to over 300 GPa) and temperatures (from 5 K to several thousand K). Coupled with synchrotron IR radiation, this facility will also provide diffraction-limited observation of diamond-cell samples in cryostats or under laser heated hot spots from the far to mid-IR spectral range. The new capabilities will greatly promote our users’ research projects to address problems ranging from outer solar system bodies to the Earth’s core, complemented by studies in materials science, condensed-matter physics, and chemistry (many of which are also carried out by the COMPRES user community).

Scientific Highlights

a. Thermally induced coloration of KBr at high pressures

The existence of defects in alkali halides under irradiation is well documented. High-intensity x-ray, UV, and infrared irradiation can generate defects that color nominally transparent

alkali halides. The most prevalent color centers in KBr are F centers, which consist of an electron trapped in a Br vacancy. Models for the radiation damage process in alkali halides include formation of F centers, aggregation of defect clusters, extended defect formation, and finally annealing, when the defects decay and return to their preirradiated condition. Extensive work at 300 K and below has been conducted to characterize the structure, properties, and timescales of defects during these stages. However, only a few studies have explored the effect of high temperatures or high pressures on color centers in alkali halides, and they have been limited to pressures < 17 GPa. In these studies, defects were introduced into the samples by irradiation prior to applying pressure. KBr is an insulator with a band-gap of 7.6 eV, too large for direct electronic excitations from the valence band into the conduction band with infrared or visible light. However, F centers acting as electron donors cause electronic states in the band gap that affect optical properties and, in particular, absorption and emission characteristics. Defect-related electronic changes are important for characterizing material performance, as KBr is used widely in optical devices. F centers in salts under planetary conditions may allow novel characterization of planetary and lunar surfaces. Changes in absorption behavior are also crucial to temperature measurements in laser-heated diamond anvil cell (LHDAC) experiments which often use KBr and other alkali halides as thermal insulation media.

LHDAC experiments led by Sarah Arveson of Yale University reveal electronic changes in KBr at pressures between ∼13–81 GPa when heated to high temperatures that cause runaway heating to temperatures in excess of ∼5000 K. The drastic changes in absorption behavior of KBr are interpreted as rapid formation of high-pressure F-center defects. The defects are localized to the heated region and thus do not change the long-range crystalline order of KBr. The results have significant consequences for temperature measurements in LHDAC experiments and extend the persistence of F centers in alkali halides to at least 81 GPa. Because of the ubiquitous use of KBr and other alkali halides in LHDAC experiments as insulation and/or as a pressure medium/calibration standard, its coloration at high pressures and temperatures is of special concern to our understanding of high-energy density physics.

Figure 1. Left: Optical images of defect-damaged sample labeled as KBr02s1 during decompression. Images were taken while at pressure in a LHDAC using both reflected and transmitted light. (a) Before heating, only the metal foil, used as a laser absorber, is visible in the gasket hole, surrounded by transparent KBr. (b) When heated on the tip of the metal foil, the KBr becomes absorbing, and the entire heated region of KBr darkens. (c)–(f) Upon decompression, the defect-damaged KBr becomes less absorbing, progressing from black to orange, to blue after the B2 to B1 phase transition at ∼1.8 GPa, and eventually returning to transparent at room pressure. Right: High-pressure visible absorbance spectra for defect damaged KBr samples (KBr07s1, FeSi923s1, KBr08s2, KBr10s1) after quenching from high temperature. The thickness of the defect damaged region is 1 μm. Unheated and un-defected KBr, regardless of the pressure, remains transparent in the wavelength range considered.

Reference:  S. Arveson, B. Kiefer, J. Deng, Z. Liu and K.M. Lee, Thermally-Induced Coloration of KBr at High Pressures, Phys. Rev. B: Condens. Matter, 97, 094103 (2018).

b. Reaching Metastability via Isothermal Pressure Pathways

Materials in metastable states, such as amorphous ice and supercooled condensed matter, often exhibit exotic phenomena. To date, achieving metastability is usually accomplished by rapid quenching through a thermodynamic path function, namely, heating−cooling cycles. However, heat can be detrimental to organic-containing materials because it can induce degradation. Alternatively, the application of pressure can be used to achieve metastable states that are inaccessible via heating−cooling cycles. Now, a team of scientists co-led by Dr. Gang Liu from HPSTAR and Dr. Jue Gong of Northern Illinois University report attainable states in 2D organic−inorganic hybrid solar perovskites reached through structural amorphization under compression followed by recrystallization via decompression. They focused on structural and related optical properties of organic-inorganic hybrid perovskites using high pressure techniques and found new metastable states in 2D hybrid perovskites using compression-decompression processes under ambient temperature. The optical absorption studies performed in the IR Lab at NSLS-II indicate that such pressure-derived metastable states in 2D hybrid perovskites exhibit enduring bandgap narrowing by as much as 8.2%, the largest pressure-driven change among all reported solar perovskites with stability under ambient conditions. The achieved metastable states in 2D hybrid perovskites via compression-decompression cycles offer an alternative pathway toward manipulating the properties of these “soft” materials with special performance. Further x-ray diffraction experiments explain that the narrowed bandgap is the result of widened Pb-I-Pb bond angles from recrystallization during decompression. The study suggests the possibility that other energy materials could have similar metastable states with improved properties when they undergo compression-decompression processes. Therefore, this study may provide a new path for obtaining metastability with unexpected properties in known materials.

Reference: G. Liu, J. Gong, L. Kong, R. Schaller, Q. Hu, Z. Liu, S. Yan, W. Yang, C. Stoumpos, et al., Isothermal pressure-derived metastable states in 2D hybrid perovskites showing enduring bandgap narrowing, Proc. Natl. Acad. Sci. USA, 115 (32) 8076-8081 (2018).

Figure 2. Pressure-dependent bandgap and structural evolution of (BA)2(MA)2Pb3I10 (n = 3) under compression-decompression cycle. (A) Tauc plots before compression (blue) and after the decompression (red), with 8.2% ambient bandgap narrowing observed. (B) XRD pattern measured after decompression from 27 GPa. (C) Comparison of enthalpy per unit cell before compression (as prepared) and after decompression (pressure treated). (D) Tauc plot for the same decompressed (BA)2(MA)2Pb3I10 (n = 3) sample but exposed to wet air (65% relative humidity) for 1 wk. (E) Comparison of bandgaps measured during compression (hollow blue dots) and decompression (solid yellow dots) under various pressures. Yellow lines are guides to the eye showing the bandgap trends during decompression. (F) Diffraction pattern images measured during compression and decompression processes.

Beamline Personnel

The management team is headed by PIs Russell J. Hemley and Zhenxian Liu of the The George Washington University. GWU serves as the funding host for the subaward of COMPRES-NSF Cooperative Agreement.

Beamline Scientist

Zhenxian Liu was appointed Research Scientist/Beamline Scientist at Carnegie in 2000, and in July 2017, he was appointed Associate Research Professor at The George Washington University. He has provided scientific and technical support to the high-pressure synchrotron IR facilities at the NSLS-U2A beamline over 15 years. He has a strong background in spectroscopy, solid-state physics, and multiple synchrotron techniques. He actively develops novel experimental techniques (e.g., vacuum far-IR spectroscopy down to 30 cm-1 at high pressure and cryogenic or external/laser heating techniques with DACs between 5-3000 K and up to 360 GPa, far-IR reflectivity spectroscopy over megabar pressures, and off-line CO2 laser heating for DACs) and assists users in carrying out research projects in a wide range of fields including geoscience, planetary science, materials science, condensed matter physics, and chemistry. In addition, he uses synchrotron infrared spectroscopy, Raman scattering and photoluminescence as well as synchrotron x-ray diffraction techniques to explore physical and chemical properties and phase transitions of hydrous minerals, simple molecular systems, and nanoscale materials under extreme P-T conditions. As the transition period from NSLS to NSLS-II is ending and the normal operation of FIS beamline with synchrotron IR source will begin soon, his work and responsibilities include:

- Coordinate with NSLS-II staff on beamline construction/developments at NSLS-II as the lead beamline scientist of FIS, the successor of NSLS-U2A. The current focus is the completion of the beam delivery pipe system and bringing the first synchrotron IR light into the front end station.  In addition, starting the beamline science commissioning at the end of the year and getting the safety approval of the newly installed laser interlock system to allow the operation of CO2 laser at the front end station are key priorities;

- Manage and provide user support during routine operations with conventional IR sources at the beamline. Current available GU time is equivalent to 50% of the total beam time.

Junior Beamline Scientist

Science commissioning at FIS will start in December 2018 followed by the start of synchrotron IR beamline operations in early 2019. We requested an increase in the FIS operation funds to support a junior beamline scientist last year but only received half of the requested funds. We request that the FIS operation funds for Year 3 will continue to support the junior beamline scientist for six months so that we can begin the hiring process. This is critical to utilize the FIS facility more efficiently and productively, as well as to continue to explore and support the DAC programs at other x-ray beamlines at NSLS-II. A candidate search and hiring process will begin as soon as the funds are committed.

Beamline Operations

A continuing effort has been made to maintain operations of the IR Lab as well as the FIS beamline at NSLS-II using conventional IR sources for COMPRES users. We have successfully moved the entire facility’s equipment from the IR Lab and cage storage area to the FIS cabins right after the FIS beamline beneficial occupancy was approved. The FIS beamline was officially opened for general users in April 2018 using the conventional sources. All required documents and forms have been approved and moved from the IR Lab to FIS beamline and user proposals have been reviewed and allocated time as General User Proposals (GUP). General users are able to use two end stations simultaneously at FIS, significantly increasing the efficiency for each visit. Our effort will focus on the beamline science commissioning and beginning beamline operations using the synchrotron IR source as soon as possible.

Beamline Community Activities: Summary of the Workshop on Synchrotron Infrared Spectroscopy on Materials in Extreme Environments

Sponsored by COMPRES and the NSLS-II Users’ Executive Committee (UEC), the workshop on Synchrotron Infrared Spectroscopy on Materials in Extreme Environments was held at NSLS-II, Brookhaven National Laboratory on May 22-23 during the 2018 NSLS-II & CFN User Meeting. We are grateful to the members of the COMPRES EOID and Executive Committee for supporting the IR workshop. This workshop brought together synchrotron-IR users to discuss the applications of high-pressure IR spectroscopy in geoscience and planetary science as well as condensed matter physics and materials science. These spectroscopic techniques for materials in extreme conditions exploit the unique instrumentation at NSLS-II, which is available to the user community. These capabilities include 1) ultra-high pressure far and mid-IR spectroscopy along with Raman, visible and other optical methods, 2) the combination of extremely low/high temperatures and pressures, 3) THz, infrared and optical spectroscopy in magnetic fields up to 10T. The workshop was a great success in terms of the quality of the lectures, broad attendance, extensive program, and user experiments arranged before and after the workshop.

The workshop consisted of two parts each afternoon on May 22 and 23, with four sessions designed to accommodate the broad range of attendees from experts to students, postdocs, and new users. The first session on May 22 focused on not only modern synchrotron IR spectroscopy techniques but also on several x-ray beamlines with the potential to accommodate DAC techniques. L. Carr (NSLS-II, Brookhaven National Laboratory) gave a tutorial overview on IR spectroscopy and the first synchrotron IR beamline project at NSLS-II. He also gave a talk on capabilities of the MET beamline (Magnetospectroscopy, Ellipsometry and Time-Resolved Optical Spectroscopies Beamline) with the potential to incorporate high magnetic field and high-pressure techniques at the beamline. Z. Liu (The George Washington University) gave an overview of the high-pressure synchrotron IR program at NSLS and NSLS-II including the current beamline capabilities and future developments. A. Fluerasu (lead beamline scientist, Coherent Hard X-ray beamline, NSLS-II) and A. Acerbo (beamline scientist, X-ray Fluorescence Microprobe beamline, NSLS-II) described their beamline techniques with the potential for DAC experiments. The second session on May 22 began with a talk by J. Musfeldt (University of Tennessee), who gave a comprehensive discussion on competing magnetostructural phases in a semiclassical system under pressure. O. Tschauner gave a talk on using synchrotron micro-scale probes for analyzing high-pressure inclusions in diamonds. K. Lee discussed difficulties in temperature measurement in laser-heated diamond-anvil cells, and S. Arveson presented her work on thermally induced coloration of alkali halides at high pressures.

Part Two of the workshop in the afternoon of May 23 was led by C. Agee (University of New Mexico) who gave a welcoming remarks and an overview of COMPRES. There were seven speakers who discussed different topics related the work they have done at beamline NSLS-U2A, the IR Lab at NSLS-II, beamline 1.4 of ALS, and other synchrotron facilities. These talks included: Using NSLS-II Infrared Light to Probe the Origin of Earth's Water (S. Jacobsen, Northwestern University); New Dense Hydrous Silica Phases Stable in the Earth’s Deep Mantle (D. Shim, Arizona State University); IR Spectroscopy of Hydrous Minerals at High Pressures: Implications for the Deep Earth (E. Thompson, University of Chicago); Challenges and Opportunities for IR Studies of Materials in Extreme Conditions (J. Townsend, Sandia National Laboratories); The Pressure-Temperature Dependent Anisotropic Elastic Properties of Upper Mantle Minerals and the Implications for the Composition and Dynamics in the Earth’s Interior (J. Zhang, University of New Mexico); Elasticity of Single Crystal Ice VII Synthesized in Externally-heated diamond Anvil Cells (B. Chen, University of Hawaii); Probing Structural Transformations, Chemical Reactivities and Guest-host Interactions at High Pressures using Infrared Spectroscopy and Synchrotron Radiation (Y. Song, University of Western Ontario); Infrared Reflectivity at High Pressure – A Tool for Probing Insulator Metal Transition (J. Tse, University of Saskatchewan). These talks not only addressed a broad range of problems in Earth and planetary sciences, materials science and chemistry, but also provided insight into new research directions that will be possible with techniques soon to be available at NSLS-II.

Finally, the scheduled user experiments (Amanda Clune, Nathan Harms, and Kenneth O’Neal from University of Tennessee; Ryan Klein and James Walsh from Northwestern University; John Hamilton and Jin Zhang from University of New Mexico; John Tse from University of Saskatchewan) at the FIS beamline before and after the workshop made the workshop even more productive. It also served to increase the visibility of the high-pressure DAC program at NSLS-II and the opportunity for the COMPRES user community to access other x-ray beamlines for DAC related experiments in the near future.

Figure 3. Group photo from the Synchrotron IR Workshop.

Beamline Developments:

2018 has been a crucial and exciting year for FIS as the installations for both the FIS beamline end stations and the dipole vacuum chamber for synchrotron IR beam extraction have been completed according to schedule. Here are the major beamline developments that have been achieved in 2018 so far:

a) Installation of dipole vacuum chamber for IR beam extraction and the first synchrotron IR light observed at the exit window of the ultra-high vacuum (UHV) optical extraction chamber

The upper half of dipole chamber fabrication was completed and delivered. The installation of the system including M4-M6 took place during the NSLS-II storage ring December 2017 winter shutdown period. The fabrication of the dipole chamber underwent vacuum leaking problems and installation was pushed to the second target date during the August-September storage ring shutdown in 2018. The entire optical extraction system has been successfully installed in early September following the Instrument Readiness Review (IRR) on October 16, 2018. The first synchrotron IR light was successfully extracted by the M1 mirror and delivered to the exit window through M2-M6 mirrors (see Figure 4). The calculated image at the diffusing screen versus the observed beam footprints on mirrors and diffuser is in good agreement (see Figure 5) indicating the 22IR optical extraction system is working quite well. The installation on the beam delivery pipe system to the end station is underway and initial beamline science commissioning is scheduled in December. We expect superb beamline performance with the synchrotron IR source based on the beam observation at the UHV exit window.

Figure 4. Left: Schematic of the UHV Optical Extraction – Final Design w/Environment. Right: Beam path through Optical Extraction System (Diagram rotated from previous for better view of mirrors)

Figure 5. Calculated image at diffusing screen versus the observed image. The 22IR optical extraction system is working quite well. Beam footprints on mirrors and diffuser in good agreement with calculation.

b) End Station installation and beamline developments

The construction of the FIS/MET beamline cabins began in January 3, 2017 and was completed in June 2017. Utility installations including nitrogen, helium, and argon gas supplies as well as compressed air and utility water have been completed in November. A total five optical tables (one 4’ by 10’, two 4’ by 8’, and two 4’ by 6’) have been installed at the end of 2017 following the relocation of all facility equipment and installation of FIS end stations. There are two end stations at FIS. End Station-1 (see Figure 6) consists of a Bruker Vertex 80v FTIR spectrometer, Hyperion 2000 IR microscope, a custom IR microscope system with long working distance (80 mm total), and a micro-Raman system. This end station has the capacity to allow users to carry out experiments over a broad P-T range. End station-2 includes a Bruker Vertex 80 FTIR spectrometer and a custom IR microscope for measurements at high pressure and room temperature. All the equipment became available for general users on April 1, 2018.

Figure 6. Left: End Station-1of FIS including the integrated custom micro-IR system and Bruker Vertex 80V FTIR spectrometer for studies under high-pressure and low-temperature or high-P-T extreme conditions; Top: End Station-2 of FIS showing the new Vertex 80 FTIR spectrometer and a custom IR microscope for studies under high-pressure and room temperature

c) Exploring high-pressure DAC opportunities at other x-ray beamlines at NSLS-II

FIS is the dedicated DAC facility for optical spectroscopic studies under extreme conditions. It also acts a base/platform to further explore high-pressure DAC opportunities at

Figure 7. Left: LED based portable ruby pressure calibration system. This system has been used at CMS and CHX beamlines; Top: sample preparation workbench including a Leica 165C microscope and an EDM machine at FIS beamline.

other x-ray beamlines as we can provide support for both pressure calibration and sample preparation (see Figure 7). The synchrotron IR workshop during the 2018 NSLS-II Users’ Meeting made more people aware of our facility and quite a few beamlines at NSLS-II are interested in adding the DAC capabilities at their facilities. We were able to make feasibility tests at two beamlines in 2018:

CMS Beamline Parameters

Energy Range: 10 -17 keV

Flux: 1010 - 1012 ph/s

Monochromator: Ru/B4C multilayer

Energy Resolution: 0.007 (ΔE/E)

Q range: 0.003 - 5 Å-1

Spot Size: 0.05-0.5 mm (H);

0.02-0.3 mm (V)

1. First DAC experiments at CMS (11-BM) beamline

The Complex Materials Scattering (CMS) beamline at NSLS II aims to facilitate rational design and discovery of new functional materials by unraveling the relations between constituents, processing, structure, and properties. To this end, CMS provides in situ and high-throughput x-ray scattering capabilities for nanoscale and mesoscale characterization of bulk and interfacial structures of complex, hierarchical materials, including nanomaterials, soft matter, and biomolecular materials. A long-term goal of CMS is to enable materials design and discovery based on intelligent, efficient exploration of materials structure in large parameter spaces. CMS provides instrumentation for simultaneous small- and wide-angle x-ray scattering (SAXS, WAXS), giving access to complementary information over broad length scales ranging from Ångstroms to microns (Fig. 8). This capability allows in situ characterization of structural evolution under extreme pressure conditions by employing high pressure in DACs, in order to investigate the relationship between structure and mechanical properties. Figure 9 shows an example of the phase transition of PbSe nanoparticle superlattice under pressure.

X-ray

DAC

WAXS

SAXS

Figure 8. Schematic of SAXS/WAXS on DAC setup

Structural evolution of PbSe nanoparticle supercrystals under pressure

Nanoparticles behave like atoms, functionalize with surface-coating organic molecules, interact with selected solvents, and self-assemble into periodically ordered superlattices. These highly ordered NC-based solids, called supercrystals, not only possess or enhance the size- and shape-dependent properties of individual NCs but also yield novel collective properties from near-field coupling of NC arrays. As a complex material consisting of both hard cores and soft organic ligands, supercrystals poses interesting mechanical properties and structures, which can be characterized in situ by employing high pressure. In one of the DAC experiments at the CMS beamline, we used 8nm PbSe nano-spheres to self-assemble the supercrystals in the FCC lattice with a lattice parameter of 14 nm,

Figure 9. Structural evolution of PbSe supercrystal under high pressure. Top: schematic of PbSe supercrystal made by nanoparticles. Bottom: evolution of D-spacings of superlattice and atomic structure in the function of pressure

SAXS

WAXS

PbSe nanoparticle

FCC superlattice

Self-assembly

Solution process

8nm

14nm

and tracked the structural evolution in both superlattice (SAXS) and atomic (WAXS) structure under high pressure. With increasing pressure, the superlattice and atomic structure shrank gradually until the phase transition simultaneously happened at 8 GPa in both atomic and nanoscale structure: the PbSe nanoparticles transformed from fcc to orthorhombic, quite different from polycrystalline PbSe with a transition pressure of 3GPa; the superlattice presented the lattice expansion with pressure > 8 GPa, comparing to the compression at lower pressure, which suggested the ligand region was compressed and then released with the phase transition of atomic structure.

2. First DAC powder diffraction experiments at the XFM (4-BM) beamline

The X-ray fluorescence microprobe (XFM) beamline is a versatile and multi-modal X-ray fluorescence microscope designed for the characterization of elemental abundances and chemical speciation in heterogeneous samples.  XFM is optimized for spatially-resolved spectroscopy (EXAFS & XANES) in the 4 - 20 keV energy range, and also offers a polychromatic "pink" mode ideal for rapid 2D and 3D fluorescence imaging and tomography. It employs compound focusing to achieve a user-tunable spot size from 2 to 10 microns while maintaining a long working distance for physically large samples and custom in situ environmental cells such as the DAC. Feasibility tests have been done at XFM during the beamline powder x-ray commissioning. An initial result on LaB6 compressed in a DAC is shown in Fig. 10.

Figure 10. First x-ray diffraction pattern of LaB6 obtained through a DAC at ambient pressure using different beam energies: black-13 keV, red-16 keV; green-18 keV; blue-16 keV (on edge the of gasket showing the tungsten peak). The x-ray beam size was 10m  10m.

Planned Activities

Our priority for the upcoming beamline commissioning in December is to make the facility available for the COMPRES user community with the IR synchrotron source in early 2019.  Major projects will include the development of the second micro-Raman system and incorporation of the CO2 laser heating system with the custom long working-distance IR microscope. The laser interlock system has been installed by the NSLS-II control group and a Laser Safety Operation Procedure (SOP) will be developed once the laser interlock system has been certified. Ongoing development of in-situ laser heating for the DAC with synchrotron IR will become available for users as soon as all required laser safety documents have been approved by NSLS-II. These techniques will greatly benefit the COMPRES user community and enable frontier research related to geosciences and materials research once they become available. Planned activities include:

a) New micro-Raman system combined with synchrotron IR spectroscopy for studies under high pressure and low temperature

We are planning to purchase an IsoPlane SCT Imaging spectrograph (Princeton Instruments, $36 K) through CDAC equipment funds. This will enable us to have two independent micro-Raman system simultaneously running at two end stations and greatly enhance the efficiency of the beamline.

b) Laser Induced Emission Spectroscopy at High P-T Conditions

While awaiting completion of the laser interlock system, the CO2 laser heating system has been installed on the optical table at End Station-1 (see Figure 11). We also relocated the Bruker IFS 66v FTIR spectrometer on the sample table. Our plan is to get both systems up and running once the required safety documents have been approved and then combined them to provide the laser induced emission spectroscopic system at high P-T conditions. The idea is to use the laser heated hot spot in a DAC as a source to the FTIR spectrometer and obtain useful information, such as phonon modes at high P and T.

Figure 11. Schematic of the existing CO2 laser heating system together with the Bruker IFS 66v FTIR spectrometer. A MgSiO3 Enstatite sample was transformed to the perovskite phase under high P-T conditions using the CO2 laser heating system.

Budget

Actual and anticipated spending for beamline operations (May 2018– June 2019):

1.  Budget for Beamline Operations:  June 2018-May 2019

| Personal: Beamline Scientists* | Salary plus fringe benefits | $215,433 | This includes a normal raise and cost of living adjustment for the senior beamline scientist and six-month support for a junior beamline scientist |
| --- | --- | --- | --- |
| Materials/Supplies a. | NSLS-II fees & stockroom | $7,757 | Routine beamline expenses including office spaces, phone charges, and materials related to the FIS end stations development. |
| Travel | Travel for senior personnel | $3,000 | Travel between BNL and Washington and to attend annual COMPRES and other scientific meetings |
|  | Total direct cost | $226,190 |  |
| Total |  | $285,000 | This total includes indirect costs** at a rate of 26% ($226,1901.26). |

* Fringe benefits: The GWU’s fringe benefit rate is 25.7%. Fringe benefits include normal costs associated with employment such as retirement, Social Security, Medicare, disability insurance, health insurance and other required taxes. Salaries are based on a full calendar year and include all leave taken.

** Indirect costs: The off-campus indirect cost rate is 26.0% of total modified direct costs (TMDC). Total modified direct costs are calculated as total direct costs minus equipment, and participant support Costs.

2. Budget Request for Beamline Operation:  June 2019-May 2020

| Personal: Beamline Scientists* | Salary plus fringe benefits | $221,896 | This includes a normal raise and cost of living adjustment for one senior and one junior beamline scientists |
| --- | --- | --- | --- |
| Materials/Supplies a. b. | NSLS-II fees & stockroom Diamond anvils and heating cell accessories | $9,656 $6,000 | Routine beamline expenses including office spaces, phone charges, and materials such as liquid helium Type IIa anvils and parts for external heating DACs required for dedicated use for high P-T experiments at the facility |
| Travel | Travel for senior personnel | $4,000 | Travel between BNL and Washington and to attend annual COMPRES and other scientific meetings |
|  | Total direct cost | $241,552 |  |
| Total |  | $304,356 | This total includes indirect costs** at a rate of 26% ($241,5521.26). |

* Fringe benefits: The GWU’s fringe benefit rate is 25.7%. Fringe benefits include normal costs associated with employment such as retirement, Social Security, Medicare, disability insurance, health insurance and other required taxes. Salaries are based on a full calendar year and include all leave taken.

** Indirect costs: The off-campus indirect cost rate is 26.0% of total modified direct costs (TMDC). Total modified direct costs are calculated as total direct costs minus equipment, and participant support Costs.

Appendices

1. A publication list for 2017 and 2018:

Arveson, S.M., B. Kiefer, J. Deng, Z. Liu and K.M. Lee, Thermally-Induced Coloration of KBr at High Pressures, Phys. Rev. B: Condens. Matter, 97, 094103 (2018).

H. Chen, M. Li, K. Leinenweber, V. Prakapenka , M. Kunz , H. Bechtel , Z. Liu and S. Shim, Stabilization of Dense Silica Phase in Hydrous Mid-Mantle Regions, Nature, submitted

Duan, P., X. Li, T. Wang, B. Chen, S. Juhl, D. Koeplinger, V. Crespi, J. Badding and K. Schmidt-Rohr, The Chemical Structure of Carbon Nanothreads Analyzed by Advanced Solid-State NMR, J. Am. Chem. Soc., 140(24), 7658-7666 (2018).

Hong, F, B. Yue, X. Wang, Z. Cheng, Z. Wang, M. Kunz, Z. Liu, B. Chen, and H.K. Mao, Pressure and Structure Driven Topological Insulator-Metal Transition in 2D Bi2Se3 Nanoflakes, Nature Materials, submitted.

Hwang, H., D. Seoung, Y. Lee, Z. Liu, H. Liermann, H. Cynn, T. Vogt, C. Kao, H. Mao, A role for Subducted Super-Hydrated Kaolinite in the Earth’s Deep Water Cycle, Nature Geoscience, 10, 947-953 (2017).

Liu, G., J. Gong, L. Kong, R. Schaller, Q. Hu, Z. Liu, S. Yan, W. Yang, C. Stoumpos, et al., Isothermal pressure-derived metastable states in 2D hybrid perovskites showing enduring bandgap narrowing, Proc Natl Acad Sci USA, 115 (32) 8076-8081 (2018).

Ke K., Y. Chen, K. Yin, J. Yan, H. Zhang, Z. Liu, J. Tse, J. Wu, H. Mao, B. Chen, Large Bandgap of Pressurized Trilayer Graphene, Nature Commun., submitted

Nisr C., S. Shim, K. Leinenweber, A. Chizmeshya, V. Prakapenka, C. Prescher, S. Tkachev, Y. Meng and Z. Liu, Geophysical Implications of Dense Polymorphs in Si1xH4xO2, Nature Commun., submitted.

O'Bannon, E.F., "High-pressure studies of subduction zone related mineral phases," Doctoral Dissertation, University of California Santa Cruz, Santa Cruz, CA, 2017, advisor Quentin Williams. 12.2.2,11.3.1,1.4

O'Neal, K., A. Clune, N. Harms, S. Cheong, J. Yang, Z. Liu, T. Birol, J. Musfeldt, High-pressure spectroscopic investigation of multiferroic Ni3TeO6, Phys. Rev. B: Condens. Matter, 98, 184101 (2018).

O'Neal K., J. H. Lee, M. Kim, J. L. Manson, Z. Liu, R. S. Fishman, and J. L. Musfeldt, Competing Magnetostructural Phase in a Semiclassical System, NPJ Quantum Materials, 2, 1-7 (2017).

O'Neal K., A. Clune, N. Harms, S. Cheong, J. Yang, Z. Liu, T. Birol and J. Musfeldt, High pressure spectroscopic investigation of multiferroic Ni3TeO6, Inorg. Chem., submitted.

Xi, X., X. Bo, X. Xu, P. Kong, Z. Liu, X. Hong, C. Jin, G. Cao, X. Wan, G. Carr, Honeycomb lattice Na2IrO3 at high pressures: A robust spin-orbit Mott insulator, Phys. Rev. B: Condens. Matter, 98, 125117 (2018).

Zhang H., Q. Li, B. Cheng, Z. Guan, R. Liu, B. Liu, Z. Liu, X. Li, T. Cui, and B. Liu, Structural Transitions and Metallization of Monoclinic Vanadium Dioxide under High Pressure, J. Phys. Chem. C., submitted.

Zhang, J., Y. Sorb, H. Deng, H. Xiao, B. Chen, R. Sereika, X. Yin, C. Yi, D. Yan, Y. Shi, Z. Liu, C. Chen, J. Chang, Y. Ding and H.K. Mao, Lattice Frustration in Spin-Orbit Mott Insulator Sr3Ir2O7 at High Pressure, Nature Materials, submitted.

2. List of users & affiliations

a) Users who performed experiments at FIS beamline, NSLS-II since November 2017:

Yale University: Kanani Lee, Sarah M. Arveson and Kiersin Daviau;

Northwestern University: Ryan Clein, James Walsh, Elizabeth Thompson and Hannah Bausch;

University of Tennessee: Janice Musfeldt, Amanda Clune, Nathan Harms and Kennth O’Neal;

University of California, Berkeley: Lucy Darago;

New Jersey Institute of Technology: Andrei Sirenko, Taras, Trevor Tyson, and Sizhang Liu;

Florida International University: Jiuhua Chen;

University of Saskatchewan, Canada: John Tse;

Yonsei University, Korea: Huijeong Hwang, Yoonah Bang, Jinhyuk Choi, Mihye Kong, and Taehyun Kim;

Sungkyunkwan University, Korea: Jungseek Hwang, Yu-Seong Seo, Seukli Roh, and Myounghoon Lee;

University of Warsaw: Jakub Gawraczynski;

HPSTAR, China: Jian Chen, Jiajia Feng, Hengzhong Zhang, Weixin Liu, Xingjian Xu, Hailun Wang, Lisa Liu, Arthur Liu, Zhiqiang Chen, Mingzhi Yuan, Ruilian Tang.

b) Mail-in users at the FIS, NSLS-II

Northwestern University: Alisha N. Clark and Steve Jacobsen;

University of Hawaii: Feng Zhu and Bin Chen

3. General user proposals for FIS beamline (FIS) received since May 1, 2018:

| Proposal ID | Title | PI | Cycle | Status |
| --- | --- | --- | --- | --- |
| 302919 | How do local lattice distortions trigger magnetic crossovers in molecule-based multiferroics? | Janice Musfeldt | 2018-2 | Closed |
| 302982 | PUP-2016-0037: Frontier Synchrotron Infrared Spectroscopy Beamline Dedicated to Optical Studies under Extreme Conditions | Russell Hemley | 2018-2 | Closed |
| 303017 | High-pressure spectroscopic studies on antiperovskite Re-Gd2SnC | Jungseek Hwang | 2018-2 | Closed |
| 303142 | Hydrogen bonding in lower mantle phases | Lily Thompson | 2018-2 | Closed |
| 303168 | Ferroelectricity in SrTiO3 nanoparticles: Pressure and Temperature Dependent IR and Raman Measurements | Trevor Tyson | 2018-2 | Closed |
| 303309 | In-situ infrared spectroscopy experiments for the pressure- and heat-induced super hydration of hydrous aluminous layered minerals | Huijeong Hwang | 2018-2 | Closed |
| 302919 | How do local lattice distortions trigger magnetic crossovers in molecule-based multiferroics? | Janice Musfeldt | 2018-3 | Allocated Time |
| 302982 | PUP-2016-0037: Frontier Synchrotron Infrared Spectroscopy Beamline Dedicated to Optical Studies under Extreme Conditions | Russell Hemley | 2018-3 | Allocated Time |
| 303067 | Synchrotron Infrared spectroscopy on small molecular systems at ultra-high pressures | Zhenxian Liu | 2018-3 | Allocated Time |
| 303142 | Hydrogen bonding in lower mantle phases | Lily Thompson | 2018-3 | Allocated Time |
| 303493 | Hydrogen incorporation in silicon oxycarbide materials | Kierstin Daviau | 2018-3 | Allocated Time |
| 303505 | High-pressure spectroscopic studies on pressure-induced superconductors, BaFe2Se3 and BaFe2S3 | Jungseek Hwang | 2018-3 | Allocated Time |
| 303511 | High Pressure Metallization of Sulfur | Sarah Arveson | 2018-3 | Allocated Time |
| 303548 | Absorption Spectroscopy as a Probe for High-Pressure Modification of Electronic Structure in Metal–Organic Frameworks | Lucy Darago | 2018-3 | Allocated Time |
| 303595 | Wavelength-dependent Absorption of Mantle Silicates and Oxides | Kanani Lee | 2018-3 | Allocated Time |
| 303609 | High Pressure mid- and far- IR Studies of compounds synthesized via hard x-ray photochemistry | Michael Pravica | 2018-3 | Allocated Time |
| 303652 | Ferroelectricity in SrTiO3 nanoparticles | Trevor Tyson | 2018-3 | Allocated Time |
| 303660 | IR study of FeOOH at high pressure | Jiuhua Chen | 2018-3 | Allocated Time |
| 302919 | How do local lattice distortions trigger magnetic crossovers in molecule-based multiferroics? | Janice Musfeldt | 2019-1 | Allocation |
| 302982 | PUP-2016-0037: Frontier Synchrotron Infrared Spectroscopy Beamline Dedicated to Optical Studies under Extreme Conditions | Russell Hemley | 2019-1 | Allocation |
| 303067 | Synchrotron Infrared spectroscopy on small molecular systems at ultra-high pressures | Zhenxian Liu | 2019-1 | Allocation |
| 303309 | In-situ infrared spectroscopy experiments for the pressure- and heat-induced super hydration of hydrous aluminous layered minerals | Huijeong Hwang | 2019-1 | Allocation |
| 303493 | Hydrogen incorporation in silicon oxycarbide materials | Kierstin Daviau | 2019-1 | Allocation |
| 303511 | High Pressure Metallization of Sulfur | Sarah Arveson | 2019-1 | Allocation |
| 303895 | High-pressure infrared optical spectroscopy study of the iron-selenide (FeSe) derived high-Tc superconductors | Xubin Ye | 2019-1 | Allocation |
| 303909 | The dehydration of hydrous ringwoodite at high pressures | Lily Thompson | 2019-1 | Allocation |
| 303962 | Raman scattering and IR reflectivity of multiferroic materials at low temperatures | Taras Stanislavchuk | 2019-1 | Allocation |
| 303964 | High-Pressure Optical Absorption for Structure-Property Relationships in Halide Double Perovskites | Nathan Wolf | 2019-1 | Allocation |
| 303969 | Ferroelectricity in SrTiO3 nanoparticles: Pressure and Temperature Dependent IR and Raman Measurements | Trevor Tyson | 2019-1 | Allocation |
| 303972 | IR spectroscopy and potential metallization at high pressure of a novel high-entropy sulfide | Hengzhong Zhang | 2019-1 | Allocation |
| 304000 | In situ IR to Probe the REAL ENVIRONMENTS of Metal Centers in Porous Metal Organic Framework | Zhiqiang Chen | 2019-1 | Allocation |
| 304075 | A Pressure-Induced Topological Quantum Phase Transition in antimony sulfide | yating jia | 2019-1 | Allocation |
| 304125 | High Pressure mid- and far- IR Studies of compounds synthesized via hard x-ray photochemistry | Michael Pravica | 2019-1 | Allocation |