Annual Report and Renewal Request for COMPRES Multi-Anvil Cell Assembly Development

Kurt Leinenwebera, James A. Tyburczyb, and Thomas G. Sharpb

aDepartment of Chemistry and Biochemistry, Arizona State University

bSchool of Earth and Space Exploration, Arizona State University

The multi-anvil cell assembly development program has existed since the beginning of COMPRES.  The concept was formulated at the original La Jolla meeting: to have a community project for developing multi-anvil cell assemblies that would ease the burden on individual laboratories and allow the sharing of designs.  Prior to that, it was not easy to get specific and precise information on cell designs – the exact ceramics used, the methods of fabrication, the precise dimensions – and some laboratories were having difficulty or taking a long time to get their new multi-anvils up and running.  Meanwhile, the multi-anvil devices themselves were proliferating because the economical Walker design had made them widely available to University laboratories.

The project proceeded to develop a number of cell assembly designs and publish their specifications.  Once the specifications were published (and to a great extent even before) it was not necessary to keep any of the methods or designs secret.  What has developed now under the guidance of the COMPRES Infrastructure Development Committee is a long-running project with a number of standard cell designs for different pressure and temperature ranges.   The cell designs are listed in Table 1.  The standardized designs are sold at cost to the community.  To give a sense of the activity in the project, the prices of each assembly and the number sold in the last fiscal year, FY14 (June 1, 2013 – May 31, 2014) is given.  Table 2 then shows the laboratories that have been using the cell designs.  It will be noted that both beam line and offline activities are represented.  In addition to the standard designs, we have also provided partial assemblies, including pieces that are not part of our standard designs and are specified by the recipient.  The standard assemblies are self-perpetuating because the cost covers the assemblies themselves plus enough overhead to run the project.  The overhead rate is 54% (it is already included in the assembly prices shown).

New developments continue to be pursued, and this is the purpose of the request for continued funding from COMPRES.

New developments in FY2014

An important area of progress in 2013-2014 was in DIA assemblies for beam line use.  This continued from FY13 when we first developed methods for making DIA designs for the NSLS beamline following the closing of the Stony Brook machine shop.  We took over the fabrication of all the DIA assemblies (D-DIA, ultrasonic DIA, and high P-T DIA) for this project, and also applied some of our methods to the fabrication of parts so that not all of them had to be made on a lathe or in a local machine shop; many of the parts are made outside by the same vendors used for the COMPRES assemblies.  This year, we helped Paul Raterron and Nadege Hilairet in the development of a new D-DIA assembly for ESRF.  This assembly has been working well and we are continuing to fabricate them for each beam time.

At the same time, we continued to provide beam line assemblies to the effort at GSECARS.  Several popular assemblies for the Large-Volume Press at GSECARS are made by our project, including rhenium heater assemblies for higher pressures and graphite heater assemblies for lower pressures.  The highly absorbing parts of the assemblies (zirconia, lanthanum chromite, and rhenium) have windows cut into them and filled by graphite or MgO pieces.  The assemblies with equatorial windows allow full access to the sample for falling sphere and other experiments needed good visibility in radiographic images, while the vertical window assemblies allow access to diffraction and partial views of the sample, but very good thermal insulation and pressure capabilities (up to the peak conditions of 25 GPa and 2000 degrees C).  GSECARS used several tens of assemblies for each beam cycle this year.

A major development that impacts COMPRES has been our work on a new pressure standard that can be used to easily and accurately calibrate assemblies.  The pressure standard is based on the solubility of SiO2 in rutile-structured  GeO2.  The volume change when SiO2 goes from coesite into this solid solution is large and negative, which means that the pressure effect on solubility is strong and the solubility can be easily evaluated by powder x-ray diffraction.  We used the COMPRES 18/12 assembly to calibrate this pressure standard, and will be making the standard available for COMPRES users.  Two papers on the system are in press or in prep (Gullikson et al., in press; Leinenweber et al., in prep).

A new development that came to fruition in 2014 was the completion of development of an electrical conductivity cell or in situ electrical measurements under pressure.  Dr. Anne Pommier (financially supported as an Exploration Postdoctoral Fellow by the ASU School of Earth and Space Exploration) undertook the very significant task of developing a well-functioning electrical conductivity assembly for use to 14 GPa and 2000 degrees C.  The group paid run charges, but additional money was needed to develop the parts and pieces that were specialized, and the COMPRES project assisted with that.  International collaboration with Bayreuth (Bayerisches GeoInstitut) helped with the design and the learning of methods for electrical conductivity measurements, which were then applied to the COMPRES assemblies.  One new development by us was to fabricate sample sleeves (MgO or other non- electrically conducting materials) with square holes because some samples to be studied were square prismatic in shape. The ASU machine shop developed a carbide broach that could be used to create a square-shaped hole by pushing it through the crushable piece along a pre-existing round hole.  Most recently, we have been pushing it only partway through the piece which makes the tiny samples and electrodes easy to load into the assembly because they sit right in the bottom of the square part of the hole and over the smaller, round hole.  The two measurement wires can then be brought in from both ends.  The electrical conductivity cell and its development will be made available through the COMPRES project.  Two papers resulting from this are in submission or in prep (Pommier et al., under review; Pommier and Leinenweber, in prep.).  (Note that one can also envision using the square hole to hold various microfabricated pieces that are square in shape for “designer experiments”).

Developments desired for FY15

Inspired partly by the conversion of this project to a Facility, we will begin some new initiatives for this project, to make it more facility-like and also to introduce new benefits to the community.

The first is to start a new initiative to provide pressure calibrants to the community for their multi-anvil cells.  We are fortunate to have a world-class inorganic chemistry laboratory next to our multi-anvil laboratory, the group of Don Seo in ASU Chemistry (note that KL is an employee of the Chemistry Department).  KL is also involved in a new project on glasses with several glass experts including Jeffrey Yarger at ASU, Robert Mayanovic at Missouri State, and Richard Weber at Containerless Leviatation.  We have not previously taken adequate advantage of these capabilities for the COMPRES project.  Our plan is to build a suite of materials that the community can use to calibrate their presses.  In the first year, we would target the new GeO2-SiO2 calibrant that has been calibrated at ASU for the range 3-9 GPa (Leinenweber et al., in preparation).  We plan to make well-characterized forsterite, enstatite, CaGeO3, ZnSiO3, and others that are frequently used high-temperature calibrants.  These could be made as gels, glasses, and/or crystalline materials depending on what is best for each type of calibration.  In order to allow reversals (which are more accurate) we will make some high pressure phases to mix together for brackets: coesite, stishovite, Mg2SiO4 beta phase and spinel, CaSiO3 garnet and perovskite.  These could be provided only in the quantities needed for calibrations because they are difficult to make.  Use of standard calibrants by different groups will represent a major step forward in inter-laboratory consistency for multianvil high pressure work.

A second is to become more involved in the issue of sample containment.  So far we have been providing “empty” cell assemblies with only a few possible sample containers (graphite, BN, porous MgO, and alumina capsules).  We have also made molybdenum capsules on spec for several laboratories.  But in our own research, our sample containment is far more sophisticated than this (as it is probably in many laboratories).  We would like to become more proactive on the sample containment issues, becoming involved with precious metal capsules, single-crystal MgO and other materials, tantalum and moly cans, etc.  We will start working with deep-drawn cup extruders, with companies like Heraeus who do precious metals, Princeton Scientific who do single-crystal capsules, and with Tracy Paul at Depths of the Earth in nearby Cave Creek, to enhance our encapsulation capabilities.

In terms of the assemblies themselves, a main direction that we will go in the next year is in the direction of larger assemblies.   There has been a call in the community for large samples of high-pressure phases, large single crystals, or large sintered bodies made at high pressure.  One aspect of this is the discussion of whether the United States should host a very large press for scaled-up multi-anvil experiments.  We can start to anticipate this by developing larger assemblies – these will also be of benefit for labs with regular-sized presses.  We already have  a 25/15 assembly as part of the COMPRES series (Stoyanov et al., 2010), but the cost of the zirconia thermal insulation sleeves is prohibitive because only a few of them can be made from an expensive block of zirconia.  We will by-pass this problem by creating a cell of porous mullite, because the mullite itself is nearly as thermally insulating as zirconia.  We think we can create a low-cost, large-volume cell by doing this.  Funding is requested for more molds for making the octahedra for this new assembly; porous mullite can be molded at Ceramco for less than ten dollars per octahedron.  There is a significant level of community interest in these large cells, which should go to 7 GPa in a normal-sized 1000 ton multi-anvil press.  Even larger assemblies can be envisioned especially when larger anvil cubes (32 mm or larger) are used as in some laboratories.

Ceramco has told us that molds with two sets of thermocouple slots, one on each end, are feasible, and we would like to make one of these this year.  This would be used for any run requiring wiring from both ends:  two-thermocouple experiments, electrical conductivity, or experiments with a second probe inside besides the thermocouple.  This year we would try this with the 8 mm size assembly, which is large enough to allow more probes to be used, but small enough to reach fairly high pressures (up to 15 GPa).

For the DIA assemblies, we will make some more shapes that have been requested by users (these are generally cubes or spheres, so molds are less costly than octahedra).  Also, we have been making a lot of the DIA parts in small batches while the project is new, but we would like to develop some of them into standard parts made outside.  Finally, there is the stubborn question of finding a better way to make boron epoxy shapes, and we will pursue a solution to this so that we can provide these shapes (pressure media) instead of each laboratory having to make their own as they do now.  We will also add boron epoxy/boron nitride windows through the gaskets and pressure media in our assemblies that are used in the large-volume press at GSECARS, in order to improve access to the low-energy region of the energy dispersive diffraction pattern, and will test them offline to assure that they perform well during beam times.

To improve the evaluation and understanding of cell assemblies, we request $15K in capital for a Labview automation system that will allow us to automatically compress, heat, and decompress while collecting detailed data on oil pressure, voltage, and amperage (and thus resistance and power).  This request includes a new computer, D to A converter cards, and some additional micropumps and pressure equipment on the presses themselves.  We have been doing without such a system for many years, but feel that the COMPRES developments will benefit greatly from being able to see subtle patterns in our experiments that we cannot see by watching a thermocouple reader, or that happen when we are out of the room, and we can also do more cell assembly testing if the presses are easier to use.  To make these developments possible, we are tweaking the funding arrangement to allow for more development work.  First, laboratory assistant Craig Naseyowma spends half his time in the laboratory supporting this development project and the other half working on materials supply storekeeping and packing for the standard cell assembly project, but his salary has been supported entirely by the development project.  It is appropriate that his salary be redistributed to the benefit of COMPRES.  We have received permission from RTS to shift half of his salary to the RTS account, instead of being paid from the COMPRES project.  This will free up money for the development effort.  We continue to request the other half of his salary from COMPRES – this will allow him to work on the developments described above – calibrating assemblies, helping with the preparation and characterization of the new community calibrants, etc. KL will be fully involved in these efforts as well.

Funding model

The funding for the two distinct aspects of this project deserves some further specific explanation.  The sale of cell assemblies is funded by the purchasers of the assemblies and is overseen by RTS (Research Technical Services) at ASU, and is run as a so-called Cost of Sales project.  An advantage of this has been that RTS is actually willing to pay for materials and supplies up front, meaning that we can buy the specialty ceramics and components of the cell assemblies and then recover the money later by selling them.  This is very difficult to do without significant financial help, especially for the larger orders.  In order to convince them to keep doing this, the budget has to be balanced at the end of each fiscal year.  However, during the fiscal year it can go quite dramatically into the negative.  In FY14, the balance on the RTS account for many months was below -100 K.  At the end of the year the balance was slightly above 0 K.  The money was all recovered by selling the materials and supplies in a timely manner before the fiscal year end.  We do most of the purchasing of materials at the beginning of the fiscal year to allow this to happen (this fiscal year so far we have spent over $200 K on cell assembly materials that will be sold this year – remember, this is RTS money, not COMPRES money).

In addition to the recovered costs, there is a 54% overhead dictated by RTS.  They use this overhead to recover a part of my salary, and starting next May they will also use it to recover half of Craig Naseyowma’s salary.  However, this money is not necessarily lost to the laboratory, either.  The RTS has a competition every year for Capital improvements.  Last year we contributed $60 K to salary recovery, but we also received two Capital improvement projects worth about the same amount.  One is allowing us to refurbish Holloway’s old gas vessel laboratory, which will also benefit the COMPRES project with further sample preparation abilities.

Budget request

The new budget request breaks down as follows:

We are requesting $15 K for new molds for pressure media, new ceramics development, and new fabrication development for multi-anvil cell assemblies.  A mold for octahedra with holes and slots is about $3 K; for DIA cubes and other simpler shapes it is less than $1K.  Each mold can be used to make about 100,000 pieces (none of our molds have worn out so far).  The molds are stored at Ceramco in New Hampshire where the parts are made.  For ceramics development, we will make test extrusions of zirconia for a less expensive zirconia option, especially important for larger cells.  Du-co ceramics is the best option for helping us with this study.

We are requesting $10 K for setting up inorganic chemistry capabilities (with the assistance of Don Seo’s group) and for chemical reagents for making a suite of pressure standards for allowing people to calibrate their multi-anvil assemblies with common calibrants.  We wish to make significant quantities of these materials, similar to how standards are made in other fields, for consistency over longer time periods as well as between laboratories.

$5K under “Facility Use Fees” is for multi-anvil run charges, analytical charges (which could be x-ray diffraction, SIMS, IR, Raman, SEM, and/or electron microprobe) for analyzing cell assemblies and minerals/materials for this project.

The Travel budget is for travel to the annual COMPRES meeting, to AGU, and to beam lines for work related to this project.

As mentioned in the text, $15 K in Capital funding is requested for an updated and improved automation system for the multi-anvils at ASU.  This will be set up using Labview and will allow full datalogging which will help to improve the development of cell assemblies by allowing a more detailed view of their operation.

The salary request is for one month of KL’s salary (KL is on a 12-month Calendar year appointment) and 6 months of Craig Naseyowma’s salary.  CN will spend half his time on the development project requested here, and the other half on the Standard Cell Assembly project.

Attachments:  1.  Budget spreadsheet.

Three primary publications

Stoyanov, E.; Haussermann, U.; Leinenweber, K. (2010)  Large-volume multianvil cells designed for chemical synthesis at high pressures.  High Pressure Research 30, 175-189.

Leinenweber, K.; Mosenfelder, J.; Diedrich, T.; Soignard, E.; Sharp, T.G.; Tyburczy, J.A.; Wang, Y. (2006):  High-pressure cells for in-situ multi-anvil experiments.  High Pressure Research 26 (3): 283-292.

Leinenweber, K.; Tyburczy, J.A.; Sharp, T.G.; Soignard, E.; Diedrich, T.; Petuskey, W.B.; Wang, Y.; Stoyanov, E.; Nite, J.; Mosenfelder, J (2012).  Development of a series of cell assemblies for reproducible multi-anvil experiments (the COMPRES assemblies).  American Mineralogist 97, 353-368.

Publications from 2011 on that reference the three primary papers on cell assemblies

2011

Couvy, H.; Lahiri, D.; Chen, J.; Agarwal, A.; Sen, G. (2011) Nano-hardness and Young's modulus of nano-polycrystalline diamond, Scripta Materialia, 64, 1019-1022.

Couvy, H.; Cordier, P.; Chen, J. (2011) Dislocation microstructures in majorite garnet experimentally deformed in the multianvil apparatus, American Mineralogist, in press.

Long, HB., Weidner D.J., Li, L., Chen, JH. and Wang, LP., (2011), Deformation of Olivine at Subduction Zone Conditions Determined from In situ Measurements with Synchrotron Radiation, Physics of the Earth and Planetary Interiors, doi: 10.1016/j.pepi.2011.02.006 (in press)

Mrosko M. Koch-Müller M., Schade U. (2011) In-situ Mid/Far-Micro-FTIR spectroscopy to   trace pressure-induced phase transitions in Sr-anorthite and wadsleyite. American Mineralogist (online). DOI: 10.2138/am.2011.3731

Schollenbruch, K.; Woodland A.B.; Frost D.J.; Wang Y.; Sanehira T.; Langenhorst F. (2011) In situ determination of the spinel – post-spinel transition in Fe3O4 at high pressure and temperature by synchrotron X-ray diffraction. American Mineralogist, in press.

Spektor, K; Nylen, J; Stoyanov, E; Navrotsky, A; Hervig, RL; Leinenweber, K; Holland, GP; Haussermann, U (2011)  Ultrahydrous stishovite from high-pressure hydrothermal treatment of SiO2.  Proceedings of the National Academy of Sciences of the United States of America.  108, 20918-20922.

Wunder B. Wirth R., Koch-Müller M. (2011) The 3.65 Å phase in the system MgO-SiO2-H2O: synthesis, composition and structure. American Mineralogist 1207 - 1214. Doi 10.2138/am.2011.3782.

2012

Puhakainen, K; Benson, D; Nylen, J; Konar, S; Stoyanov, E; Leinenweber, K; Haussermann, U (2012)  Hypervalent Octahedral SiH62- Species from High-Pressure Synthesis.  Angewandte Chemie International Edition 51, 3156-3160.

Tenner, TJ; Hirschmann, MM; Withers, AC; Ardia, P (2012)  H2O storage capacity of olivine and low-Ca pyroxene from 10 to 13 GPa: consequences for dehydration melting above the transition zone  Contributions to Mineralogy and Petrology 163, 297-316.

Wu, Y; Litvinchuk, AP; Toberer, ES ; Snyder, GJ; Newman, N; Fischer, A; Scheidt, EW; Scherer, W; Haussermann, U (2012) Thermoelectric properties of Zn5Sb4In2-delta (delta=0.15).  Journal of Applied Physics 111, Article Number 123712

2013

DuFrane, W.L., Sharp, TG; Mosenfelder, JL; Leinenweber, K (2013)  Ringwoodite growth rates from olivine with similar to 75 ppmw H2O: Metastable olivine must be nearly anhydrous to exist in the mantle transition zone.  Physics of the Earth and Planetary Interiors 219, 1-10.

Eklof, D; Fischer, A; Wu, Y; Scheidt, EW; Scherer, W; Haussermann, U  (2013)  Transport properties of the II-V semiconductor ZnSb.  Journal of Materials Chemistry 4, 1407-1414.

Jacobsen, MK; Liu, W; Li, B  Measurement setup for the simultaneous determination of diffusivity and Seebeck coefficient in a multi-anvil apparatus.  Review of Scientific Instruments 83, Article number 093903.

Otsuka, K.; Longo, M.; McCammon, C.A.;  Karato, S.I.  (2013)  Ferric iron content of ferropericlase as a function of composition, oxygen fugacity, temperature and pressure: Implications for redox conditions during diamond formation in the lower mantle  Earth and Planetary Science Letters 365, 7-16

Rainey, E.S.G.; Hernlund, J.W.; Kavner, A. (2013)  Temperature distributions in the laser-heated diamond anvil cell from 3-D numerical modeling.  Journal of Applied Physics 114, Article Number 204905.

Righter, K; Danielson, LR; Pando, K; Morris, RV; Graff, TG; Agresti, DG; Martin, AM; Sutton, SR; Newville, M; Lanzirotti, A (2013) Redox systematics of martian magmas with implications for magnetite stability.  American Mineralogist 98, 616-628.

Tian, YJ; Xu, B; Yu, DL; Ma, YM; Wang, YB; Jiang, YB; Hu, WT; Tang, CC; Gao, YF; Luo, K; Zhao, ZS; Wang, LM; Wen, B; He, JL; Liu, ZY (2013)  Ultrahard nanotwinned  cubic boron nitride.  Nature 493, 385-388.

Zeilinger, M.; van Wuellen, L.; Bensen, D.; Kranak, V.F.; Konar, S.; Fassler, T.F.; Haussermann, U. (2013)  LiBSi2: A tetrahedral semiconductor framework from boron and silicon atoms bearing lithium atoms in the channels.  Angewandte Chemie – International Edition 52, 5978-5982.

Zhang, Y.F.; Wang, Y.B.; Wu, Y.; Bina, C.R.; Jin, Z.M., Dong, S.W. (2013)  Phase transitions of harzburgite and buckled slab under eastern China.  Geochemistry Geophysics Geosystems 14, 1182-1199.

2014

Al-Khatatbeh, Y; Lee, KKM (2014)  From superhard to hard: A review of transition metal dioxides TiO2, ZrO2, and HfO2 hardness.  Journal of Superhard Materials 36, 231-245.

Jacobsen, M.K.; Liu, W.; Li, B. (2014)  Enhancement of thermoelectric performance with pressure in Ce0.8Fe3CoSb12.1.  Journal of Physics and Chemistry of Solids 75, 1017-1023.

Jing, Z.C.; Wang, Y.B.; Kono, Y.; Yu, T.; Sakamaki, T.; Park, C.; Rivers, M.L.; Sutton, S.R.; Shen, G.Y. (2014)  Sound velocity of Fe-S liquids at high pressure: Implications for the Moon's molten outer core.  Earth and Planetary Science Letters 396, 78-87.

Pommier, A. (2014)  Interpretation of Magnetotelluric Results Using Laboratory Measurements.  Surveys in Geophysics 35, 41-84.

Scwartz, M.R.; Antlauf, M.; Schmerler, S.; Keller, K.; Schlothauer, T.; Kortus, J.; Heide, G.; Kroke, E.  (2014)  Formation and properties of rocksalt-type AlN and implications for high pressure phase relations in the system Si-Al-O-N.  High Pressure Research 34, 22-38.

Gullikson, A.; Leinenweber, K.; Stoyanov, E.; Zhang, H.; Malik, A.-S. (in press).  High Pressure Investigation in the System SiO2-GeO2: Mutual Solubility of Si and Ge in Quartz, Coesite, and Rutile-type phases.  In press, Journal of the American Ceramic Society.

Leinenweber, K.; Gullikson, A.; Stoyanov, E.; Malik, A.-S. (in preparation).  Solubility of SiO2 in argutite (GeO2 rutile) as a precise ex-situ pressure standard from 3 to 10 GPa.  In preparation for Journal of Materials.

Pommier, A.; Leinenweber, K.; Kohlstedt, D.L.; Qi, C.; Garnero, E.J.; Mackwell, S.J.; Tyburczy, J.A. (In preparation)  Experimental constraints on the electrical anisotropy of the lithosphere-asthenosphere system.  Submitted to Nature.

Pommier, A.; Leinenweber, K. (in preparation).  Experimental Investigation of the Electrical Behavior of Olivine during Partial Melting under Pressure.  In preparation for Earth and Planetary Science Letters.

Table 1.  Participating laboratories.

| Institution | Location | Contact(s)/Advisors | Last 12 months |
| --- | --- | --- | --- |
| Aarhus University | Aarhus, Denmark | Martin Bremholm |  |
| Argonne National Laboratories | Lemont, IL | Tamas Varga |  |
| Arizona State University | Tempe, AZ | Kurt Leinenweber |  |
| Australian National University | Canberra, Australia | Robert Rapp |  |
| Bayerishches Geoinstitut | Bayreuth, Germany | Dan Frost |  |
| Brookhaven National Laboratories | Brookhaven, NY | Matthew Whitaker |  |
| Brown University | Providence, RI | Stephen Parman, Geertje Ganskow |  |
| California Institute of Technology | Pasadena, CA | Jed Mosenfelder (moved to Minnesota) |  |
| Carnegie Institution of Washington, Geophysical Laboratory | Washington, D.C. | Valerie J. Hillgren, Li Zhang, Yingwei Fei |  |
| Case Western Reserve University | Cleveland, OH | James Van Orman, Katherine Crispin |  |
| China University of Geosciences | Wuhan, China | Zhenmin Jin |  |
| Chinese Academy of Sciences | Beijing, China | Changqing Jin, L. Sun |  |
| Columbia University, Lamont-Doherty Earth Observatory | Palisades, NY | David Walker, Wei Du |  |
| COMPRES Technology Center (COMPTECH) | Argonne, IL | Bin Chen |  |
| Delaware State University | Dover, DE | Gabriel Gwanmesia |  |
| Florida International University | Miami, FL | Jiuhua Chen, Helene Couvy |  |
| GFZ Helmholtz-Zentrum Potsdam | Hamburg, Germany | Monika Koch-Muller, Hans J. Mueller |  |
| Institute for Geowissenschaften, Universität Frankfurt | Frankfurt, Germany | Alan Woodland |  |
| IPGP | Paris, France | James Badro, Julien Seibert |  |
| Jilin University | Changchun, China |  |  |
| Los Alamos National Laboratories | Los Alamos, NM | Jianzhong Zhang |  |
| LSPM-CNRS | Villetaneuse, France | Petr. Sokolov |  |
| Lawrence Livermore National Laboratories | Livermore, CA | Julien Siebert (moved to IPGP) |  |
| Macquarie University | Sydney, Australia | Simon Clark |  |
| Massachusetts Institute of Technology | Cambridge, MA | William B. Durham, Nathaniel Dixon |  |
| NASA Johnson Space Center | Houston, TX | Lisa Danielson |  |
| National Cheng Kung University | Tainan, Taiwan | Jennifer Kung |  |
| Northern Illinois University | DeKalb, IL | Heather Watson |  |
| Observatoire Midi-Pyrénées | Toulouse, France | Frédéric Béjina |  |
| Seoul National University | Seoul, Korea | Eun Jung Kim |  |
| Starwave Technologies | San Jose, CA | Hong Yu |  |
| Stony Brook University | Stony Brook, NY | Baosheng Li, Hongbo Long, Li Li, Simon Hunt |  |
| Texas A&M University | College Station, TX | Caleb Holyoke |  |
| Toshiba Tungaloy America | Itaska, IL | Ron Pang |  |
| Universite Lille (and ESRF) | Villeneuve d'Ascq, France | Paul Raterron, Nadège Hilairet |  |
| University College London | London, England | Rachel Haezel, Paul F. McMillan |  |
| University of Amsterdam | Amsterdam, The Netherlands | Wim van Westrenan |  |
| University of Arizona | Tucson, AZ | Kenneth Domanik |  |
| University of California at Davis | Davis, CA | Charles Lesher, Alisha Clark, Lara O’Dwyer Brown |  |
| University of Chicago,GSECARS | Argonne, IL | Yanbin Wang, Tony Yu |  |
| University of Colorado | Boulder, CO | Joseph Smyth |  |
| University of Hawaii | Honolulu, HI | Murli Manghnani |  |
| University of Michigan | Ann Arbor, MI | Jie Li |  |
| University of Minnesota | Minneapolis, MN | Shenghua Mei, Jed Mosenfelder |  |
| University of New Mexico | Albuquerque, NM | Laura Burkemper, Carl Agee, Karen Hutchins, Stephen Elardo, Valerie Burkemper, Kathleen Vanderkaaden |  |
| University of Nevada at Las Vegas | Las Vegas, NV | Pamela Burnley, Shanmin Wang |  |
| University of Western Ontario | London, Ontario, Canada | Richard A. Secco |  |
| Yale University | New Haven, CT | Kazuhiko Otsuka, Justin Hustoft, George Amulele, Shun-ichiro Karato |  |
| Yanshan University | Qinhuangdao, China | Dongli Yu |  |

Table 2: Multi-anvil assemblies developed and standardized by the COMPRES project, and other items

| Assembly name | Peak pressure | Proven temperature | Design | Cost per assembly for FY13 (COMPRES users) | Number ordered in last 12 months (Orders 271-320) |
| --- | --- | --- | --- | --- | --- |
| 8/3 | 25 GPa | 2319 °C | Rhenium furnace | $59.87 | 790 |
| 10/5 | 20 GPa | 2000 °C | Rhenium furnace | $70.69 | 790 |
| 14/8 “G2” | 13 GPa | 1200 °C | Graphite box furnace | $81.90 | 370 |
| 14/8 step heater | 15 GPa | 1400 °C | Graphite step furnace | $81.90 | 45 |
| 14/8 “HT” | 15 GPa | 2200 °C | Rhenium furnace | $70.00 | 80 |
| 18/12 | 9 GPa | 1500 °C | Graphite box furnace | $110.75 | 210 |
| 8/3 window assembly in-situ | 25 GPa | 2200 °C | LaCrO3 sleeve and rhenium furnace with windows | $59.87 | 20 |
| 10/5 window assembly in-situ | 20 GPa | 2200 °C | LaCrO3 sleeve and rhenium furnace with windows | $70.69 | 32 |
| 10/5 equatorial assembly in-situ | 20 GPa | 1700 °C | TiB2+BN straight furnace, MgO equatorial window, mullite octahedron. | $70.69 |  |
| 14/8 “G2” in-situ | 13 GPa | 1200 °C | Graphite box furnace, forsterite sleeve | $81.90 | 0 |
| 14/8 equatorial assembly in-situ | 15 GPa | 1500 °C | TiB2+BN step furnace, MgO equatorial window, mullite octahedron | $81.90 | 30 |
| Spherical D-DIA assembly | 6 GPa | 1700 °C | Based on Durham sphere and seat | (Made to order: machining cost) | 40 |
| D-DIA (Deformation DIA) | 8 GPa | 1400 °C | Stony Brook design made at ASU | (Made to order: machining cost) | 50 |
| U-DIA (Ultrasonic DIA) | 8 GPa | 1400 °C | Stony Brook design made at ASU | (Made to order: machining cost) | 50 |
| DIA (regular DIA for diffraction) | 8 GPa | 1400 °C | Stony Brook design made at ASU | (Made to order: machining cost) | 50 |
| Odd parts: molybdenum capsules, parts |  |  |  |  | 758 |
| Accessories: nesting plates, dummies, etc. |  |  |  |  | 41 |
| Anvils truncated |  |  |  |  | 682 |